## Slide 1
ATTENTION: See Adjustment for AIA/ICC
When presenting for AIA credits, unhide slide 4
When presenting for ICC credits, unhide slide 5

## Slide 2
Insert Full Page
Image Here
UTILIZING MASS TIMBER METAL CONNECTORS EFFECTIVELY

## Slide 3: Credit Information
IACET Accreditation Information
Simpson Strong-Tie® has been accredited as an Authorized Provider by the International Association for Continuing Education and Training (IACET). As a result of their Authorized Provider accreditation status, Simpson Strong-Tie® is authorized to offer IACET CEUs for its programs that qualify under the ANSI/IACET Standard.
This course offers 0.1 CEU (1 hour of credit).
Notes: Review the submission process for audiences requiring IACET CEU credits.
For those seeking IACET credit, they must take and pass the online test. They must self-report CEU credits to their certifying organization or agency.
Explain the credits awarded: IACET: 0.1 (Equivalent to 1 hour) CEUs.

## Slide 4: Utilizing Mass Timber Connectors Effectively
Simpson Strong-Tie
PO Box 10789, Pleasanton, CA 94588
https://www.strongtie.com/
The American Institute of Architects
Course No. AIA-MTC12023This program qualifies for
1.0 LU/HSW Hour
Course Expiration Date:
06/01/2026
VIEW DETAILS
Simpson Strong-tie is a registered provider of AIA-approved continuing education. All registered AIA CES Providers must comply with the AIA Standards for Continuing Education Programs. Any questions or concerns about this provider or this learning program may be sent to AIA CES (cessupport@aia.org or (800) AIA 3837, Option 3).
This learning program is registered with AIA CES for continuing professional education. As such, it does not include content that may be deemed or construed to be an approval or endorsement by the AIA of any material of construction or any method or manner of handling, using, distributing, or dealing in any material or product.
AIA continuing education credit has been reviewed and approved by AIA CES. Learners must complete the entire learning program to receive continuing education credit. AIA continuing education Learning Units earned upon completion of this course will be reported to AIA CES for AIA members. Certificates of Completion for both AIA members and non-AIA members are available upon completion of the test.

## Slide 5: Utilizing Mass Timber Connectors Effectively
Simpson Strong-Tie
PO Box 10789, Pleasanton, CA 94588
https://www.strongtie.com/
International Code Council (ICC)
Course No. 36760
This program qualifies for
.1 CEU (1 Hour of Credit)
Course Expiration Date:
06/01/2026
VIEW DETAILS
This course has been approved by the International Code Council (ICC) for continuing professional education.
For learners that complete this course, it is your responsibility to self-report your credits to the ICC. Please retain your Completion Certificate for your records.
Be sure that your ICC ID number is provided on the sign-in sheet or in your Simpson profile in order to have it displayed on your certificate.

## Slide 6: Purpose and Learning Objectives
Purpose:
This course provides an overview of mass timber construction and its various framing approaches with a focus on metal connectors and fasteners.
Learning Objectives:
At the end of this program, participants will be able to:
describe mass timber carbon capture, indoor environmental quality, and safety benefits
specify the most appropriate metal connectors
compare various types of mass timber framing systems, and
utilize metal connectors as structural and design elements.
Notes: Mass timber is a construction methodology that effectively integrates environmental responsibility, improved building performance, and the many benefits of off-site construction. This course provides an overview of recent and rapid advancements in this field and reviews mass timber components and the various framing approaches that can be utilized. It focuses on the metal connectors and fasteners that enable the system to function solidly and elegantly.
Learning Objectives:
At the end of this program, participants will be able to:
describe how mass timber construction impacts carbon emissions, indoor environmental quality, and safety
specify the most appropriate metal connectors when designing mass timber structures, considering fire ratings, constructability, shrinkage and swelling, and moisture protection
compare types of mass timber framing systems for cost and speed of construction, seismic resistance, carbon emissions, and clear span, and
utilize metal connectors as structural and design elements simultaneously.

## Slide 7: Agenda
Introduction
CLT Construction: Systems and Applications
Mass Timber Connectors and Fasteners
Mass Timber Systems
Summary
KK Law, courtesy naturallywood.com

## Slide 8: INTRODUCTION
KK Law, courtesy naturallywood.com

## Slide 9: What is Mass Timber?
Mass (massive) timber uses engineered components of smaller wood pieces bonded together into large structural elements.
Mass timber components can be as strong as concrete and steel.
Components are manufactured off-site and assembled quickly, cleanly, and accurately on-site.
Mass timber is different from heavy timber which basically uses solid lumber.
Notes: Mass (massive) timber is a structural framing system that uses engineered components made with smaller wood pieces bonded together to create large floor and wall panels, posts, beams, and other structural elements.
Mass timber components can achieve the same strength as nonwood products such as concrete and steel but are much lighter. These components are manufactured off-site and assembled quickly and cleanly on-site. with high accuracy.
Mass timber is an advancement from heavy timber construction, which is generally associated with using large solid beams and columns sawn from a single log. Heavy timber can, however, use certain mass timber elements such as glulam beams.

## Slide 10: Mass Timber Benefits: Carbon Sequestration
Wood products are 50% carbon by dry weight: mass timber buildings can store carbon well into the future.
Manufacturing, transportation, and assembly processes also have a low carbon footprint.
Mass timber produces 30% fewer CO2 emissions than concrete buildings and 50% fewer than steel-frame buildings. (Turner and Townsend )
Notes: In addition to sequestering the carbon stored naturally in the trees from which mass timber products are created, the component manufacturing, transportation, and assembly processes also have a low carbon footprint. Wood products are 50% carbon by dry weight, meaning mass timber buildings can store carbon well into the future.
Turner and Townsend note that mass timber produces 30% fewer CO2 emissions than concrete buildings and 50% fewer than steel-frame buildings. Mantle Developments cites mass timber as the most carbon-efficient building material for multistory construction.
This is an essential benefit in an era when carbon capture and low or zero carbon emissions are becoming increasingly important in building design.

## Slide 11: Mass Timber Benefits: Sustainability
Mass timber wood is harvested from sustainably managed forests.
Mass timber uses small and medium-sized newer-growth trees.
Removing smaller trees from overpopulated forests is healthy for forests and reduces wildfire risk.
Mass timber can use diseased trees.
Notes: Wood products used for mass timber construction are primarily harvested from sustainably managed forests where replacement stock keeps the harvest rate at or below the forest’s new growth rate.
Mass timber uses small and medium-sized newer-growth trees to create large building components. Removing these trees from overpopulated forests supports healthy forest management and reduces wildfire risk. It also creates new markets for wood products and promotes a more sustainable future.
Mass timber uses smaller sawn pieces so that even diseased trees can be used instead of being left to decompose and release their encapsulated carbon. Because the components are made from smaller dimensional lumber, very little of each log is wasted.

## Slide 12: Mass Timber Benefits: Sustainability
Components can be reused if a building is deconstructed (i.e. design for disassembly).
Metal connectors facilitate disassembly.
The recycling/reuse potential of mass timber buildings is 73% vs. 34% for reinforced concrete. (Quiming Sun et al)
Mass timber is lighter than steel and conc., uses smaller foundations.
Exposed elements eliminate finishing materials.
Notes: In addition, the building components can be reused if a building is deconstructed at any point in its life cycle. The approach to such reuse is generally referred to as design for disassembly. The initial use of metal connectors facilitates such disassembly. One analysis by Qiming Sun et al. concluded that within a 100-year service life, the recycling/reuse potential of mass timber buildings is 73% compared to 34% for a reinforced concrete structure.
Mass timber is a lighter construction material than steel and concrete, so foundations are reduced in size. Specific components, such as columns, beams, walls, and floor panel elements, can also be left exposed to the interior, thus eliminating the need for certain finishing materials.
Reducing the number of required materials and their associated environmental impacts is another factor that improves a mass timber structure’s sustainability and environmental benefits.

## Slide 13: Mass Timber Benefits: Sustainability
Mass timber construction can reduce overall construction times up to 25%.
On-site assembly reduces framing labor by 40% to 50%, resulting in cost savings.
Mass timber panels’ R-value is 1.2 per inch.
Panels, manufactured to very close tolerances, provide airtight connections.
The visual presence of wood relaxes occupants. (UBC/FPInnovations study)
Notes: Because mass timber components are prefabricated off-site and assembled with metal connectors, they can be turned into 3D structures much more quickly on-site than other forms of construction. It is estimated that mass timber construction can reduce overall construction times by as much as 25%. The on-site assembly process also reduces framing labor by 40 to 50%, resulting in cost savings.
Wood is a poor conductor of heat and cold and, as such, also functions as an insulator that contributes to the overall energy efficiency of the building envelope. Mass timber panels, for example, have an R-value of 1.2 per inch. In addition, they are manufactured to very close tolerances in the factory setting and, when assembled, provide airtight connections.
People respond emotionally to wood and are attracted to its visual variety and natural expressiveness. A study carried out by the University of British Columbia and FPInnovations found that the visual presence of wood in a room lowers the sympathetic nervous system activation in occupants, making them feel more relaxed.

## Slide 14: Mass Timber Benefits: Acoustics
Wood is inherently sound absorbent.
Exposed floor/ceiling panels usually require additional acoustic treatment.
Options include (lightweight concrete/gypsum toppings, acoustic underlayment, or a finished floor surface set on sleepers c/w sand.
Notes: Wood has an inherent, natural ability to dampen sound. However, when mass timber floor/ceiling panels are left exposed, they usually require additional acoustic treatment to achieve the desired sound separation.
This treatment could include additional mass (lightweight concrete/gypsum toppings, as shown in the image), acoustic underlayment, or a finished floor surface set on sleepers combined with a sand topping.

## Slide 15: Mass Timber Benefits: Strength and Safety
Mass timber meets or exceeds the structural and fire performance demands of other structural materials. (IBC®)
It can achieve sufficient stiffness, strength, and ductility to resist strong winds and earthquakes.
During seismic testing, floor and wall panels show almost no damage or residual deformation.
During fires, mass timber components char on the outside while retaining strength.
Notes: Mass timber has a high strength-to-weight ratio and is recognized by the International Building Code® (IBC®) as meeting, or in some cases exceeding, the structural and fire performance demands of other structural materials. It can achieve sufficient stiffness, strength, and ductility to resist strong winds and earthquakes.
The reduced building mass is beneficial to seismic forces. During seismic testing, floor and wall panels show almost no damage or residual deformation. In 2007, a joint Italian-Japanese research team tested a seven-story CLT mass timber building on a “shake table.” They found that it could withstand the seismic forces of the 1995 earthquake in Kobe, Japan, which destroyed more than 50,000 buildings.
During fires, mass timber components char on the outside, forming a protective layer while retaining the strength of the member.

## Slide 16: Mass Timber Benefits: Aesthetics
One motivation for mass timber is the appeal of exposed wood.
Two of the new construction types allow designers to expose some or all of the interior timber framing.
Notes: Wood has an inherent, natural ability to dampen sound. However, when mass timber floor/ceiling panels are left exposed, they usually require additional acoustic treatment to achieve the desired sound separation.
This treatment could include additional mass (lightweight concrete/gypsum toppings, as shown in the image), acoustic underlayment, or a finished floor surface set on sleepers combined with a sand topping.

## Slide 17: Mass Timber Components: Cross-Laminated Timber (CLT)
CLT forms large panels using sawn boards.
Each layer is glued at 90° to the other to give structural rigidity in two directions.
Board thicknesses: ⅝″ (16 mm) to 2″ (50 mm)
Board widths: 2.5″ (63.5 mm) to 5.5″ (140 mm)
Typical applications include floors, walls, roofs, and diaphragms which transmit lateral loads to the vertical load-resisting elements.
Notes: There are several variations of mass timber components, all of which use smaller sawn lumber pieces fastened together in various ways to create larger and stronger structural elements.
CLT is one of several methods of forming large panels of 3 to 9 layers using sawn boards. For CLT, each layer is glued at 90° to the adjacent layer, resulting in structural rigidity in two directions. Board thicknesses vary between ⅝″ (16 mm) and 2″ (50 mm), and board widths range from 2.5″ (63.5 mm) to 5.5″ (140 mm).
Typical applications include floors, walls, roofs, and diaphragms, which transmit lateral loads to the vertical load-resisting elements, such as shear walls or braced frames. In most instances, CLT floor and roof decks act as rigid diaphragms.

## Slide 18: Mass Timber Components: Dowel Laminated Timber (DLT)
DLT panels are:
softwood lumber boards friction-fit together with hardwood dowels. i.e.no glue or nails
used for walls, floors, roofs, stairs, elevator shafts, or bent and curved structures.
precisely cut
capable of accommodating mechanical services and sound-absorbing insulation, and
able to be topped with concrete.
Notes: DLT panels are made from softwood lumber boards stacked on end and friction-fit together with hardwood dowels. This method uses no glue or nails. DLT panels can be used for walls, floors and roofs, stairs, elevator shafts, or bent and curved structures.
They can be easily processed and precisely cut using computerized numerical control (CNC) machinery in a factory setting. DLT panels can also accommodate mechanical services and sound-absorbing insulation and can be topped with concrete to form TCC (timber-concrete-composite) panels.

## Slide 19: Mass Timber Components: Nail Laminated Timber (NLT)
NLT wood pieces are nailed (or screwed) together.
NLT can be fabricated with readily available dimensional lumber and locally sourced materials.
NLT is used for monolithic slab panels, including curves and cantilevers.
Plywood or oriented strand board on one face provides in-plane shear capacity.
Notes: NLT is similar to DLT except that wood pieces are nailed (or screwed) together instead of dowelled. NLT can be assembled outside a factory setting since it can be fabricated with readily available dimensional lumber and locally sourced materials.
It can be used to create monolithic slab panels, including curves and cantilevers. Adding plywood or oriented strand board sheathing on one face of the panel provides in-plane shear capacity, allowing it to be used as a shear wall or structural diaphragm.

## Slide 20: Mass Timber Components: Glue-Laminated Timber (GLT)
GLT is composed of selected dimension lumber pieces bonded with durable, moisture-resistant adhesives.
Lamination grains run along beam length.
GLT can be used as columns or beams, side by side as panels or planks for floor or roof decking as well as for bridges, canopies, and pavilions.
GLT combines well with hybrid assemblies.
Notes: GLT or glulam is composed of individual dimension lumber pieces, selected and positioned based on their performance characteristics and then bonded together with durable, moisture-resistant adhesives.
The grain of all laminations runs parallel with the length of the members. Glulam members can be used as columns or beams (straight or curved) or affixed side by side as panels or planks for floor or roof decking, similar to NLT.
GLT is well suited to long-span structures and custom curvilinear shapes and can be used for major load-bearing structures such as bridges, canopies, and pavilions. It combines well with hybrid assemblies and building systems.

## Slide 21: Review Question
Mass timber construction (CLT floor panels, in particular) often requires additional treatment to meet acoustic separation requirements.
What are the treatments named in this course?

## Slide 22: Answer
Acoustic treatments could include lightweight concrete/gypsum toppings, acoustical underlayment, or a finished floor surface set on sleepers combined with a sand topping.

## Slide 23: CLT CONSTRUCTION: Systems and Applications
Michael Elkan, courtesy naturallywood.com

## Slide 24: CLT Fabrication
CLT can be made from solid-sawn structural grade 2x dimensional lumber or SCL (structural composite lumber) products such as laminated veneer lumber (LVL).
Panel thicknesses: 4½″ (115 mm) to 19½″ (495 mm)
Panel widths and lengths: 8′ (2.4 m) to 64′ (18.5 m)
Adhesives are chosen based on the requirements of the end product.
Notes: While CLT is most commonly made from solid-sawn laminations using structural grade 2x dimensional lumber, it can also be made from SCL (structural composite lumber) products such as laminated veneer lumber (LVL).
CLT panel thicknesses range from 4½″ (115 mm) to 19½″ (495 mm), and their width and length can range from 8′ (2.4 m) to 64′ (18.5 m). Thickness varies with panel dimensions and structural considerations.
The adhesives used are chosen based on the particular requirements of the end product. Some of the typical glues used include phenol-formaldehyde resin or phenolic resin (PH), phenol-resorcinol-formaldehyde (PRF), resorcinol-formaldehyde (RF), melamine-urea-formaldehyde (MUF), polyurethane (PUR), and emulsion-polymer-isocyanurate (EPI).

## Slide 25: CLT Fabrication Process
Lumber is selected
Kiln dried to 12% moisture content
Defects removed
Pieces trimmed and jointed
Solid wood layers formed in both directions
Each layer sprayed with adhesive
Panels pressed together hydraulically
Panels cut, milled, and finished
Notes: The production sequence for CLT panels is as follows:
Lumber is selected: common types include western larch and Douglas fir.
Lumber is kiln dried to 12% moisture content.
Defects are removed.
Lumber pieces are trimmed and jointed.
Boards are placed, and solid wood layers are formed in both directions.
Every layer is sprayed with an adhesive.
The panel is pressed together with a hydraulic press.
Panels are then cut to size, milled, and finished as required for each project.

## Slide 26: CLT Benefits
Alternating grains improve dimensional stability, give a strength-to-weight ratio like concrete at 20% of its weight.
They are cost-effective for multistory and long-span diaphragm applications.
CLT can be left exposed in certain 8 to
9-story Type IV-C buildings.
CLT construction is versatile, fast, clean, and comparatively quiet.
10′ by 40′
3 m by 12 m
4½″ to 19½″
115 mm to 495 mm
Major axis
Notes: Alternating grains improve CLT panels’ dimensional stability and give CLT a strength-to-weight ratio comparable to concrete but at only 20% of its weight.
The panels’ ability to resist high racking and compressive forces makes them incredibly cost effective for multistory and long-span diaphragm applications.
CLT can be left exposed in building interiors up to eight or nine stories in Type IV-C buildings under the 2021 IBC (depending on occupancy).
CLT construction is versatile, fast, and clean (there is virtually no on-site waste) and comparatively quiet.

## Slide 27: CLT Mass Timber Building Code Development
Codes have evolved at pace with advancements in CLT and mass timber construction techniques.
2015: CLT first recognized in US by IBC prescriptive code (limit of six stories (B occupancy) or 85′ (26 m)).
Dec. 2015:ICC formed an ad hoc committee and in a few years, the code allowed greater heights and areas.
Type IV-HT (heavy timber) was allowed for 324,000 ft2 in total building area with an average of 54,000 ft2/story in the 2018 IBC.
Notes: Because of the rapid advancement in CLT and mass timber construction techniques and engineering, codes have evolved quickly to match their potential abilities and benefits.
CLT was first recognized as recently as 2015 in the US by the IBC. It was defined as “a prefabricated wood product consisting of not less than three layers of solid sawn lumber or structural composite lumber where the adjacent layers are cross-oriented and bonded with structural adhesive to form a solid wood element.”
At that time, there was a prescriptive code limit of six stories (B occupancy) or 85′. In December of that year, the ICC (International Code Council) formed an ad hoc committee on tall wood buildings, and in a few years, the code allowed greater heights and areas.
Type IV-HT (heavy timber) was allowed for 324,000 ft2 in total building area with an average of 54,000 ft2/story in the 2018 IBC.

## Slide 28: CLT Mass Timber Building Code Development
2018:IBC contains nine construction types (I, II, III, IV, and V), with all but type IV having an A and B type.
Buildings over six stories could obtain approval by an Alternate Materials and Methods Request (AMMR).
2021: IBC added three more construction types (IV-A, IV-B, IV-C) with type IV-A allowing up to 18 stories and 270′ (82 m) in height.
 | Type IV-A | Type IV-B | Type IV-C
Max. stories | 18 | 12 | 9
Max. height | 270′ (82 m) | 180′ (55 m) | 85′ (26 m)
Allowable building area | 972,000 ft2 (90,300 m2) | 648,000 ft2 (60,200 m2) | 405,000 ft2 (37.625 m2)
Average area/story | 54,000 ft2 (5016 m2) | 54,000 ft2 (5016 m2) | 45,000 ft2 (4180 m2)
Notes: In 2018, the IBC contained nine construction types (I, II, III, IV, and V), with all but type IV having an A and B type. Buildings over six stories could obtain approval by an Alternate Materials and Methods Request. (AMMR) through performance-based design.
The 202I IBC added three more construction types (IV-A, IV-B, IV-C) with type IV-A allowing up to 18 stories and 270′ (82 m) in height.

## Slide 29: CLT Mass Timber Building Code Development
2022: 284′ (86 m), 25-story Ascent MKE mixed-use building in Milwaukee, Wisconsin, officially the tallest mass timber building in the world.
Other proposals are up to 100 meters.
The building has 19 stories of mass timber on six stories of concrete.
Approvals took two years.
Notes: As of 2022, the 284′ (86 m), 25-story Ascent MKE mixed-use building in Milwaukee, Wisconsin, (images) was officially the tallest mass timber building in the world. However, there were also proposals to build as high as 100 meters.
The building consists of 19 stories of mass timber on top of six stories of concrete, with two concrete elevator shafts used as a lateral-force-resisting system.
The structural team provided performance-based design and fire testing to get approvals, which took two years.

## Slide 30: Review Question
How many mass construction types did the IBC recognize in 2018, and what were they?

## Slide 31: Answer
In 2018, the IBC contained nine construction types (I, II, III, IV, and V), with all but type IV (heavy timber or HT) having an A and B type.

## Slide 32: MASS TIMBER CONNECTORS AND FASTENERS

## Slide 33: Connection Classes
Class 1 connections require only mass timber elements and structural fasteners and to be fire resistant (per National Design Specification® (NDS®) for Wood Construction)
Class 2 connections are custom steel-fabricated elements: plates, angles, and structural fasteners. They require additional fire protection.
Class 3 connections are prefabricated proprietary connectors mainly using wood to
protect the steel connector.
  often backed by supporting strength tests and either have a specified fire rating
  or require additional protection.
Notes: Connection design must consider structural design, aesthetics, fire ratings, constructability, shrinkage and swelling, and moisture protection. Connections are grouped into three broad classes.
Class 1 connections require only mass timber elements and structural fasteners and must be fire resistant according to the National Design Specification® (NDS®) for Wood Construction calculations.
Class 2 connections are custom steel-fabricated elements comprising components such as plates, angles, and structural fasteners. They require additional fire protection.
Class 3 connections are prefabricated proprietary connectors from suppliers, mainly using wood to protect the steel connector. They are often backed by supporting strength tests and either have a tested and specified fire rating or require additional protection to meet fire rating requirements.

## Slide 34: Connection Types: Spline Joints
Spline joint
A shallow rabbet receives a narrow plywood strip flush with the panel surface and connected to two adjacent panels with screws.
Splines are typically ¾″ (19 mm) to 1⅛″ (28.6 mm) thick and approximately 6″ (120 mm) wide but can be up to 10″ (25.4 cm) wide.
This is a common edge joint connection for a floor or roof panel.
Notes: Because there are many structural conditions and configurations, there are also many specialized connectors specifically designed to be used with each one.
A variety of panel connectors are presented, arranged from least expensive to most expensive. Panel connectors deal with the transfer of in-plane shear and tension along the panel to the panel joint.
Spline joint: A shallow rabbet is routed in at the top of each mating panel, and a narrow plywood strip is fastened across the joint in the field. The plywood is installed flush with the panel surface and connected to two adjacent panels with a series of screws at a spacing determined by the connector designer. The plywood splines are typically ¾″ (19 mm) to 1⅛″ (28.6 mm) thick and approximately 6″ (120 mm) wide. (Splines can be up to 10″ (25.4 cm) wide when an aggressive fastening pattern is required.) This is considered the most common and versatile edge joint connection for a floor or roof panel.

## Slide 35: Connection Types: Steel Surface Straps
Surface steel straps are fastened to two adjacent panels by screws.
Straps provide a tensile connection across wood components.
Exposed floor straps require a finished floor.

## Slide 36: Connection Types: Half-Lap Joints, Butt Joints, Tube Connectors
Half-lap joint: CLT panels are routed to half depth, overlapped, and secured with screws inserted through horizontal portion. Joint is used beside a side cantilever where it must resist uplift.
Butt joint: Specialized screws are inserted at a 35° to 40° angle from both sides.
Tube connectors: Adjacent floor panels are butted and secured with slotted steel tubes and glued-in threaded rods.
Notes: Half-lap joint: Both sides of the CLT panels are routed to half the depth and then overlapped together before securing the joint with screws. One series of screws is inserted through the horizontal portion of the overlapping wood to hold the panels together. A half-lap joint is appropriate adjacent to a side cantilever where the joint must resist uplift.
Butt joint: Specialized screws are inserted at a 35° to 40° angle from each side of the joint at a spacing determined by the system designer.
Tube connectors: Adjacent floor panels are butted together and secured using slotted steel tubes and glued-in threaded rods.

## Slide 37: Panel Support at Beams: Floor-to-Beam Connections
Floor-to-beam connections transfer vertical loads from the panel to the beam.
Type 1: Panels screwed directly to beam. Designer determines screw types etc.
Type 2: Panel rests on beam recess, secured with screws at a 35° to 40° angle from each side.
Type 3: Ledgers screwed to the side of the beams, panels fastened to them with vertical screws.
Notes: Floor-to-beam connections transfer vertical loads from the panel to the beam.
Type 1: Panels are screwed directly to the beam. The system designer determines the screw types and spacings.
Type 2: Panels rest on recesses cut in the top of the beam and are secured with screws at a 35° to 40° angle from each side.
Type 3: Additional dimensional members (ledgers) are screwed to the side of the beams, and the panels rest on those ledgers and are fastened to them with vertical screws.
Other steel connectors could also be used; however, they are not as economical.

## Slide 38: Floor Panel-to-Wall Panel Connections
These transfer vertical loads from floor or roof panels to wall panels, and transfer in-plane and out-of-plane shear between wall and floor panels.
Ledger connection, balloon framing: Screws secure the floor panel to the ledger attached to the wall panel.
Metal bracket, balloon framing: Floor panels are connected to an L-shaped metal bracket secured to the wall panel.
Concealed plates: Floor panels rest on the horizontal portion of T-shaped connectors inserted into wall panels.
Notes: Floor panel-to-wall connections transfer vertical loads from floor or roof panels to a vertical wall panel. They also transfer in-plane and out-of-plane shear between wall and floor panels.
Ledger connection, balloon framing: A lumber ledger piece is attached to the wall panel, and screws secure the floor panel to the ledger top.
Metal bracket, balloon framing: An L-shaped metal bracket is secured to the wall panel, and the floor panel rests on and is connected to the bracket. The bracket can be mounted with the “L” upside right or upside down.
Concealed plates: T-shaped connectors are inserted into the wall panels with the leg of the T vertical in the panel. Floor panels rest on the wall panel, and the horizontal portion of the T is fastened through the floor panel.

## Slide 39: Fasteners
Partially threaded fasteners are available in lengths of up to 360 mm (14-3/16″).
Fully threaded fasteners are available in lengths up to 600 mm (23⅝″).
Each fastener type is designed for particular tasks.
System designers should consult manufacturers’ catalogs to see the full range.
Notes: As with metal connectors, there is a wide selection of fully threaded and partially threaded screws for mass timber construction. Partially threaded fasteners (screws) are available in lengths of up to 360 mm (14-3/16″).
Fully threaded fasteners are available in lengths up to 600 mm (23⅝″). Each fastener type is designed for particular tasks.
This course illustrates just a few representative examples most closely aligned with the fastener and joint types noted earlier.
System designers should consult manufacturers’ catalogs to see the full range of options.

## Slide 40: Fasteners
Countersunk fully threaded screws:
For beam reinforcement, wall-to-wall and floor-to-floor connections, support beams, and butt joints, CLT and mass timber construction, and interior applications.
Lengths: 4¾″ (120 mm) to 13¾″ (350 mm)
Countersunk partially threaded screws:
For wall-to-wall, floor-to-floor, wall-to-floor, panel-to-beam, panel-to-wall and ledger connections, surface splines, lap joints, general timber framing connections, CLT and mass timber construction, general interiors.
Lengths: 3⅛″ (80 mm) to 14″ (300 mm)
Notes: Countersunk fully threaded screws:
For beam reinforcement, wall-to-wall connections, floor-to-floor connections, support beams, and butt joints: They are available in lengths of 4¾″ (120 mm) to 13¾″ (350 mm) and are designed for CLT construction, mass timber construction, and general interior applications. They have a proprietary point that provides fast starts and excellent holding power. These screws can also be used as compression reinforcement in a beam.
Countersunk partially threaded screws:
For wall-to-wall, floor-to-floor, wall-to-floor, panel-to-beam, and panel-to-wall connections, surface splines, lap joints, ledger connections, and general timber framing connections: They are available in lengths of 3⅛″ (80 mm) to 14″ (300 mm) and are designed for CLT construction, mass timber construction, and general interior applications. They pull structural members together with super-holding power. The large, flat head with underhead nibs provides for clean countersinking.

## Slide 41: Fasteners
Hex head with recessed screw:
For CLT construction, general interior applications, and steel plate-to-wood connections.
Partially threaded, 0.394″ (10 mm) and 0.472″ (12.5 mm) diameter, structural fasteners pull structural members together.
Structural wood screw, cap head:
Excellent for butt joint and uplift resistance connections between wall plates and wall framing and top plate and roof rafters/trusses.
Fully-threaded shank.
Small diameter allows close spacing without splitting.
Notes: Hex head with recessed screw:
This structural fastener is designed for CLT construction and general interior applications and is used for steel plate-to-wood connections. These partially threaded, 0.394″ (10 mm) and 0.472″ (12.5 mm) diameter structural fasteners pull structural members together while providing excellent connection strength.
Structural wood screw, cap head:
This screw is an excellent solution for butt joints and uplift resistance connections. The full-threaded shank engages the entire length of the fastener, providing a secure connection. It is tested in accordance with ICC-ES AC233 (screw) and AC13 (wall assembly and roof-to-wall assembly) for uplift and lateral loads between wall plates and vertical wall framing and between the top plate and the roof rafters or trusses. The small diameter allows narrow spacing without causing splitting.

## Slide 42: Fasteners
Wood with variable thread screw:
Used for CLT applications: surface splines, half-lap joints, attaching sole plates to rim boards.
4″ (120 mm) long.
Structural wood screw:
For CLT construction applications and multi-plywood members.
Lengths: 215/16″ (74.6 mm) to 6⅝″ (168.25 mm).
Requires less torque than comparable fasteners.
Large washer head pulls members down.
Notes: Wood with variable thread screw:
This screw is used for CLT applications such as diaphragm surface splines and half-lap joints and to attach a sole plate to a rim board. It is 4″ (120 mm) long.
Structural wood screw:
This screw, available in lengths of 2-15/16″ (74.6 mm) to 6⅝″ (168.25 mm), is designed for CLT construction applications and multi-plywood members. It requires less torque to install than comparable fasteners. The large diameter washer head pulls members down easily, eliminating the need for extra washers.

## Slide 43: Connector/Fastener Combinations
Angle brackets:
Used to connect CLT wall panels to CLT floors or concrete slabs.
Various options are available.
Simple screwed connections:
Use based on connection capacity and wall application.
Heavy Duty Washer straps:
Used in CLT diaphragm and wall applications.
Carry tension across CLT floor or wall panel joint or anchor CLT panels to concrete.
Notes: Angle brackets:
Angle brackets are used to connect CLT wall panels to CLT floors or concrete slabs. Various fastener and anchor options are available depending on the required loads and application.
Simple screwed connections:
These can be used based on the capacity of the connection and the wall application (shear wall or bearing wall).
Washer straps:
Seven-gauge heavy-duty tension straps with high strength and stiffness are used in various CLT diaphragm and wall applications. High capacity reduces the need for expensive shop-fabricated steel plates. They carry tension across a CLT floor or wall panel joint or anchor CLT panels to concrete through welded steel attachment.

## Slide 44: Connector/Fastener Combinations
Anchor tie-down systems:
Secure midrise wood-frame buildings against overturning wind and seismic forces.
Components work together to create a continuous load path.
Built for maximum resilience and installation efficiency.
Notes: Anchor tie-down systems:
Rod tie-down systems are designed to secure midrise, wood-frame buildings against overturning forces caused by wind and seismic events.
Components work together to create a continuous load path and are built for maximum resilience and installation efficiency.

## Slide 45: Exposed Beam to Column Connectors
High-capacity face-mount hangers:
One type supports joists on wood purlins or beams.
Second type is used on 8″ (200 mm) grouted masonry block walls.
Both are ideal for high-wind applications.
Hinge connectors:
Transfer loads between two beams aligned through a combination of bearing plates, side plates, and bolts.
Can have additional slotted bolt holes to resist horizontal loads.
Notes: High-capacity face-mount hangers:
There are two variants of this type of hanger. One supports joists on wood purlins or beams. The other is used on standard 8″ (200 mm) grouted masonry block walls. These purlin hangers have enhanced uplift capacity and are ideal for high-wind applications.
Hinge connectors:
Hinge connectors transfer loads between two beams aligned end to end through a combination of bearing plates, side plates, and bolts. In addition to supporting vertical loads, hinge connectors can also be specified with additional slotted bolt holes to resist horizontal loads as part of a continuous load path.

## Slide 46: Exposed Beam to Column Connectors
Beam seats:
Connect beams to concrete or concrete masonry units.
Anchored into the concrete or masonry.
Designed for cast-in-place applications.
Provide additional bearing for beam.
Steel plate separates wood from masonry or concrete.
Available in high capacity and medium capacity.
CConcrete Pilaster
Notes: Beam seats:
These connect a beam and a concrete or concrete masonry unit and are anchored into the concrete or masonry. They are designed for cast-in-place applications.
They also provide an additional bearing for beam connections, and the steel plate provides a barrier for wood from the masonry or concrete.
These seats are available in a high capacity and medium capacity as well.

## Slide 47: Medium-Capacity Concealed Hangers
Designed for use when the header and joist are flush at floor or roof level.
Use connector screws, no predrilling required.
Provide a clean joint and fire resistance.
Provide a +/– 1/32″ (0.7 mm) beam length tolerance at each connector.
Can be routed into carrying beam or joist or not routed at all.
Notes: These hangers are designed for use when the header and joist are flush at the top of the floor or roof level.
They use connector screws to make installation fast and easy, with no predrilling required.
They provide a clean joint as well as fire resistance.
The concealed hanger design provides a +/– 1/32″ (0.7 mm) beam length tolerance at each connector, making it easy to crane into place.
The hangers can be routed into either the carrying beam or the joist or not routed into either one.

## Slide 48: High-Capacity Concealed Hangers
Machined from aluminum for a high-capacity design.
Allowable stress design load capacity of up to 20 kips.
Strongest of concealed end-grain beam hangers.
Allow for clean connection with 1 and 2-hour fire resistance (ASTM E119).
Factory installed with generous fit-up tolerance for easy beam installation.
Notes: These hangers are machined from aluminum for a high-capacity design. They have an allowable stress design load capacity of up to 20 kips and are the strongest connector of concealed end-grain beam hangers.
Their concealed connection allows for clean connection while offering 1- and 2-hour fire resistance ratings per ASTM E119.
The hanger installs easily in the factory and offers generous on-site fit-up tolerance for smooth and easy beam installation.

## Slide 49: Knife Plate Concealed Hangers
Installed in three ways:
  no header/post or beam routing
  routed header/post
  routed beam
Part of a concealed connector system with three capacities (light, medium, and high).
Connector has 30 kip max capacity.
Carried member can slope up or down to 45° with full loads.
Notes: These can be installed in three ways: with no header/post or beam routing, a routed header/post, or a routed beam.
They are part of a concealed connector system with three capacities (light, medium, and high).
The seated knife plate connector has a maximum capacity of 30 kips. The carried member may be sloped up or down to 45° with full table loads.
They are supplied with all the required dowels (short or long, based on the supported beam width) and screws.

## Slide 50: Review Question
What does a washer strap for walls or floors do?

## Slide 51: Answer
Washer straps carry tension across a CLT floor or wall panel joint or anchor CLT panels to concrete through a welded steel attachment.

## Slide 52: MASS TIMBER SYSTEMS
KK Law, courtesy naturallywood.com

## Slide 53: Column-and-Plate
Sometimes called post-and-plate.
Consists of CLT panels supported only on columns.
Column grid spacing limited by CLT’s maximum panel width.
Notes: In addition to the comprehensive range of components, connectors, and fasteners, mass timber framing systems can be configured and combined with other materials.
Column and plate:
A column-and-plate (sometimes called post-and-plate) system consists of CLT panels supported only on columns. As with most systems of construction, it has both advantages and disadvantages.
For post-and-plate systems, the column grid spacing is limited by the CLT’s maximum width that suppliers can produce or that can be transported to the site.

## Slide 54: Column-and-Plate
CLT panels are usually 12′ (3.6 m) wide. (transportation)
Best for buildings with narrow column grids (student residences, hotels).
CLT panels sized for resistance in the weaker span and at-point supports
Connections detailed to support CLT slabs onto the columns adequately.
Notes: Most plants produce CLT panels only up to approximately 12′ (3.6 m) wide, primarily because of transportation limitations. As a result, these systems are best suited for buildings that can accommodate narrow column grid spacing, such as student residences or hotels.
The system designer must consider other factors, including sizing the CLT panels to provide sufficient resistance in the weaker span and at-point supports and detailing connections to support the CLT slabs onto the columns adequately.
.

## Slide 55: Column-and-Plate
Brock Commons Tallwood House (18-story, 184′ (56 m) houses 400 students.
17 stories of column and plate on concrete podium.
Prefab steel and metal decking roof.
Framing completed <70 days,
four months faster than similar projects.
Notes: The 18-story, 184′ (56 m) high Brock Commons Tallwood House student residence at the University of British Columbia in Canada is an example of this type of framing. This building provides accommodation for over 400 students as well as study and amenity spaces.
The structure comprises 17 stories of column and plate framing (five-ply CLT panels on glulam columns) above a concrete podium. The roof is made with prefab steel sections and metal decking.
The framing was completed in less than 70 days after the prefabricated components arrived on-site, approximately four months faster than a typical project of this size.

## Slide 56: Post, Beam, and Plate
Plates rest on beams connected to columns: facilitates greater column spacing.
Spacing determined by beam capacity, not panel width.
Suited for buildings with large column grid spacing. (offices)
Reduced headroom under beams, potential conflicts between beams and services in ceiling spaces.
Lorem ipsum dolor sit amet, consectetur adipiscing elit. Cras lectus risus, tempor eu porttitor convallis, cursus id est. Aenean sollicitudin fermentum tortor, consectetur facilisis dui pellentesque sit amet. Duis lobortis viverra odio. Vivamus malesuada tortor ut egestas accumsan. Nunc id nisl eget ante interdum sagittis.
Notes: As the name suggests, this system utilizes plates resting on beams connected to columns. This arrangement facilitates a column spacing greater than that for column and plate. It is determined by the beam capacity, not the panel width.
This system is well suited for buildings requiring large column grid spacing, such as open-concept office towers or multipurpose buildings that require lots of spatial flexibility.
The drawbacks to the system include the reduced headroom under the beam and the potential conflicts between beams and mechanical or electrical services in ceiling spaces.

## Slide 57: Post, Beam, and Plate
Examples include:
Three-story Mountain Equipment Company head office building in BC using GLT columns and beams with steel connectors.
25-story Ascent building in Milwaukee (19 mass timber stories over six stories of concrete).
Used GLT post/beam/plate system.
Notes: One example of this type of framing is the three-story Mountain Equipment Company head office building in British Columbia (left images), which uses glulam columns and beams with steel connectors.
The 25-story Ascent building in Milwaukee (19 mass timber stories over six stories of concrete) was also constructed using a glulam column/beam/plate system. Two concrete cores provide lateral stability.
ost, Beam, and Plate

## Slide 58: Mass Timber and Steel Hybrid
Hybrid steel-frame/mass timber has longer beam spans, smaller column sizes than mass timber post-and-beam.
Excellent for uses such as office buildings.
Steel moment frames can be a perfect lateral-force-resisting system for high seismic regions.
Notes: A hybrid steel-frame building with mass timber floor panels allows for longer beam spans and smaller column size than comparable mass timber post-and-beam construction, making it an excellent option for uses such as office buildings. However, this system can also suit other uses.
Steel moment frames can be a perfect lateral-force-resisting system for high seismic regions.

## Slide 59: Mass Timber and Steel Hybrid
The Fast + Epp’s four-story, 17,000 ft2 is a hybrid, mass timber steel (columns) building mass The structure was erected in 12 days and uses an earthquake resistance technology that effectively dissipates energy and does not require post-event maintenance.
  The Fast + Epp’s four-story, 17,000 ft2 (1580 m2) building is a hybrid, mass timber steel (columns) structure that was erected in 12 days.
  Its earthquake resistance technology effectively dissipates energy and does not require post-event maintenance.
Notes: The Fast + Epp’s four-story, 17,000 ft2 mass timber home office in Vancouver, British Columbia, is a hybrid, mass timber steel (columns) building. In 2021, the structure was erected in 12 days. The building uses an earthquake resistance technology that effectively dissipates energy and does not require postevent maintenance. It anchors the CLT shear walls and was a first in North America.

## Slide 60: Mass Timber-Concrete Composite
Timber-concrete composite (TCC) technology: a concrete slab connected to a timber panel or beam.
Concrete resists compression, wood offers tensile strength. The concrete slab can be poured or precast.
On-site pours reduce the weight of the timber panels and create a rigid structural diaphragm.
TCC requires less concrete than conventional construction methods.
Reducing carbon-intensive concrete and increasing low-carbon timber creates a smaller environmental footprint.
Notes: Timber-concrete composite (TCC) technology, when used for reinforcement, is essentially a concrete slab connected to a timber panel or beam. The materials work together to optimize structural performance.
The concrete resists compression while the wood, with its capacity to flex, offers tensile strength. Either solid mass timber panels or engineered wood beams can be used. The concrete slab can be poured on-site or precast in a shop environment.
On-site pours reduce the weight of the timber panels due to composite action and, without additional topping, create a rigid structural diaphragm. This flat, horizontal platform transfers lateral loads to the vertical columns of the building. Electrical and mechanical systems can be integrated into the concrete layer. Another advantage of TCC technology is that it requires less concrete than conventional construction methods, shifting the load to the timber. Reducing the use of carbon-intensive concrete and increasing the use of low-carbon timber creates a smaller environmental footprint.

## Slide 61: Mass Timber and Stick Framing Hybrid
Mass timber/stick framing is a nearly all-wood hybrid with various advantages over light frame construction:
fewer on-site crew members needed
smaller carbon footprint
high building-volume-to-surface-area ratio
lighter weight and lower foundation costs
natural insulation with thermal advantages
the ability to flex during an earthquake
Notes: Mass timber combined with light-frame construction is essentially a nearly all-wood hybrid building system. It offers unique opportunities not possible with light-frame construction alone, such as a cantilevered design element.
Prefabricated mass timber with light-frame systems offer several advantages over the conventional full stick framing approach: fewer crew members needed on-site, smaller carbon footprint, a high building-volume-to-surface-area ratio for generous interiors, lighter weight, lower foundation costs, natural insulation that offers thermal advantages, and the ability to flex during an earthquake.
When mass timber is left exposed, projects have the bonus of aesthetic warmth and a biophilic benefit.

## Slide 62: Mass Timber and Steel Hybrid
Virtuoso: 10,000 m2 (107,500 ft2), six-story residential condominium at UBC.
The first building on that campus to use a light-frame and mass timber hybrid system.
Notes: The Fast + Epp’s four-story, 17,000 ft2 mass timber home office in Vancouver, British Columbia, is a hybrid, mass timber steel (columns) building. In 2021, the structure was erected in 12 days. The building uses an earthquake resistance technology that effectively dissipates energy and does not require postevent maintenance. It anchors the CLT shear walls and was a first in North America.

## Slide 63: SUMMARY
KK Law, courtesy naturallywood.com

## Slide 64: Summary
Mass timber is steadily growing in popularity and sophistication.
Components are precisely manufactured off-site and quickly assembled in the field.
Mass timber often meets or exceeds the strength and fire resistance of concrete or steel.
Buildings of 18 stories or more are now feasible and approvable.
Connections are critical.
A comprehensive range of metal connectors and fasteners is available for every building configuration and connection situation.
Notes: Mass timber construction, the creation of buildings using large components created by bonding multiple, smaller, cut-to-size pieces, is steadily growing in popularity and sophistication. Building components are manufactured to a high degree of precision off-site in a factory setting and quickly assembled in the field. This form of construction often meets or exceeds the strength and fire resistance of concrete or steel. In a relatively short period of time, the engineering of such buildings has developed to where mass timber buildings of 18 stories or more are feasible. Such buildings are now readily accepted by building codes and are being successfully constructed in greater and greater numbers around the world.
Critical to the engineering inherent in this type of construction is the manner in which the large components are connected together in the field. A comprehensive range of metal connectors and fasteners is now available to facilitate every building configuration and connection situation. Some of these connectors are visible and some are intended to be hidden. Connector options consist of a wide range of purpose-designed screws used in combination with a variety of straps, angles, brackets, tie-downs, beam seats, concealed plates, and hinge connectors—each chosen to accommodate the load and component configuration.
Designers now have the freedom to choose whether they wish to express the connections with visible connectors or whether they would prefer to hide the connectors to provide a cleaner look. In either instance, they can rely on the structural integrity of the approach.

## Slide 65: Summary
Connector options include a comprehensive range of purpose-designed screws used with a variety of straps, angles, brackets, tie-downs, beam seats, concealed plates, and hinge connectors.
Some connectors can be left visible and others are designed to be hidden.
Designers can choose to express the connections with visible connectors or hide the connectors to provide a cleaner look.
In all instances, they can rely on the structural integrity of the approach.

## Slide 66: Thank You
Questions?
This concludes the American Institute of Architects Continuing Education System Course
https://www.strongtie.com/
©2023 Simpson Strong-tie