## Slide 1
PLEASE READ
Dear Instructor,
This presentation is available in both AIA and ICC versions.
For AIA: Right click and un-hide slides 5 and 175
For ICC: Right click and un-hide slides 6 and 176
Slide 2 is an optional slide

## Slide 2: Welcome!
We will begin in a few minutes.
Please be sure to sign the registration form to receive credit for attending today’s learning event.
Notes: Do
Meet and greet participants as they arrive. Start learning names, make them feel comfortable and settled in the training environment.
Make sure your opening has PUNCH:
Promotes interest and enthusiasm for the session
Understands participants’ needs
Notes ground rules and administrative/housekeeping needs
Clarifies expectations
Helps everyone get to know each other
State your expectations around participation: Make it known and expected that you will be encouraging and inviting participation.
Tips to facilitate connections:
Thank participants for their contribution (ideally with their name)
Praise participation (especially the first person to speak)
Express confidence in the participants
Restate what someone said earlier (“As John mentioned earlier….”)
Encourage participants to share what others were saying in their small groups (without naming names)
Invite someone you heard speaking in a small group to share with the entire group
Encourage the group to respond to an individual’s comment/question
Physical Room / Training Venue Setup:
If using a table arrangement, consider grouping 4 to 6 students at each station. This will help encourage conversation and discussion during activities.
Get people standing at regular intervals during your training session. Research shows that people learn up to 15% more when standing up!

## Slide 3
Concrete Repair Design
Design Considerations for Successful Repairs
AIA Course Number:
AIA-RPSD0215
____________
AIA Provider: 50119826

## Slide 4: Credit Information
IACET Accreditation Information
Simpson Strong-Tie® has been accredited as an Authorized Provider by the International Association for Continuing Education and Training (IACET). As a result of their Authorized Provider accreditation status, Simpson Strong-Tie® is authorized to offer IACET CEUs for its programs that qualify under the ANSI/IACET Standard.
This course offers 0.2 CEU (2 hours of credit).
Notes: Review the submission process for audiences requiring IACET CEU credits.
For those seeking IACET credit, they must take and pass the online test. They must self-report CEU credits to their certifying organization or agency.
Explain the credits awarded: IACET: 0.2 (Equivalent to 2 hours) CEUs.

## Slide 5: Credit Information
AIA Member Information
This course is registered with AIA CES for continuing professional education. As such, it does not include content that may be deemed or construed to be an approval or endorsement by the AIA of any material of construction or any method or manner of handling, using, distributing, or dealing in any material or product. Upon completion of this course, Credit(s) earned will be reported to AIA CES for AIA members who pass the course and have entered their AIA member number on their Simpson profile page. A link to the Certificate of Completion will be available upon completion of this course. Only AIA LU/HSW will be reported.
This course offers 2 LU/HSW credits.
AIA Course Number: AIA- RPSD0215
Notes: Presenter Information
NOTE: Please be sure each attendee LEGIBLY signs the event sign-in sheet.
Say
All questions concerning proprietary products will be addressed after the conclusion of the AIA portion of the presentation. The meeting format is 110 minutes of content, followed by 10 minutes of Q & A.
Do
Explain the credits awarded for:
AIA: 2LU/HSW credits.
IACET: 0.2 (Equivalent to 2 hours) CEU credits.
Review the submission process for audiences requiring either AIA LU/HSW (health, safety and welfare) credits or CEU credits:
For those seeking AIA HSW credit, there is no test required. AIA members must be sure to provide their AIA member number on the sign-in sheet. Please make sure name, email and AIA member number are clearly printed so Simpson can report credits to the AIA on their behalf.
For those seeking IACET credit, they must take and pass the test. They must self-report CEU credits to their certifying organization or agency.

## Slide 6: Credit Information, cont.
ICC Member Information
This course has been approved by the International Code Council (ICC) for continuing professional education. For learners that complete this course, it is your responsibility to self-report your credits to the ICC. Please retain your Completion Certificate for your records.
Be sure that your ICC ID number is provided on the sign-in sheet or in your Simpson profile in order to have it displayed on your certificate.
This course offers 0.2 CEU (2 hours of credit).
ICC Course Number: 5742
Notes: Review the submission process for audiences requiring ICC CEU credits.
For those seeking ICC credit, there is no test required. ICC members must provide their ICC ID number on the sign-in sheet or in their Simpson profile in order to have it displayed on their certificate. It is the responsibility of the participant to self-report their credits to the ICC. Ask them to retain their Completion Certificate for their records.
Explain the credits awarded: ICC: 0.2 (Equivalent to 2 hours) CEUs.

## Slide 7: Additional Credit Offerings
Visit
strongtie.com/workshops
for more information
Course Name | CEUs | AIA | ICC
Introduction to Deck Design | 0.1 | ✔ | ✔
Introduction to Wind Design and the Wood Frame Construction Manual | 0.1 | ✔ | ✔
Shear Walls and Lateral Bracing in Light Frame Construction | 0.1 | ✔ | ✔
Understanding Restraint Rod Systems | 0.1 | ✔ | ✔
Cracking the Concrete Anchor Codes | 0.1 | ✔ | ✔
Concrete Deterioration | 0.1 | ✔ | ✔
Moment Frame Design | 0.1 | ✔ | ✔
Introduction to Wind Code Provisions and Meteorological Concepts | 0.1 | ✔ | ✔
Wind Design in Accordance with ASCE 7-10 | 0.1 | ✔ | ✔
Wood Framed Seismic Design 1: Code Provisions, Design Parameters | 0.1 | ✔ | ✔
Notes: Do
Explain that we have additional PK topics available that offer credit for ICC members and HSW credits for AIA members.
Explain that we have a library of online courses available in our Simpson Student Center that also offer ICC and AIA HSW credits. They can access our online courses at strongtie.com/workshops.

## Slide 8: Course Description
This course seeks to equip industry professionals with the resources needed to properly assess and plan a successful repair.
We will examine the various methods and materials available for the repair of concrete structures and explore the advantages and disadvantages of each depending on the job at hand.

## Slide 9: Learning Objectives
After completing this course, you will be able to:
Conduct a visual concrete condition survey
Determine the material requirements for a job
Explain the difference between different types of repair materials
Explain which material properties may be ideal for certain repairs
Identify when certain admixtures may be used in proprietary repair mortars for certain applications
Explain the advantages and disadvantages of various placement methods
Notes: Do
Review the learning objectives for the course.
Inform students that the assessment questions will be based on these learning objectives. Slides that may contain information relevant to the test have a teal graduation cap located in the bottom-left corner.

## Slide 10: Concrete Repair References
International Concrete Repair Institute
American Concrete Institute
American Society for Testing and Materials
References:
Places to go for more information will be indicated throughout the course by this magnifying glass.
Notes: Throughout this course, we will reference some standards and guidelines that you can refer to for more information. These references will be indicated by this magnifying glass. Next, we will cover a few of the major organizations in the concrete industry.

## Slide 11: Concrete Repair References
International Concrete Repair Institute
American Concrete Institute
American Society for Testing and Materials
References:
www.icri.org
International Concrete Repair Institute (ICRI)
Notes: The International Concrete Repair Institute (ICRI) is the leading resource for education and information to improve the quality of repair, restoration, and protection of concrete and other structures. This organization mainly focuses on proper repairs as opposed to how to install and erect new concrete structures.

## Slide 12: Concrete Repair References
International Concrete Repair Institute
American Concrete Institute
American Society for Testing and Materials
References:
American Concrete Institute (ACI)
www.concrete.org
Notes: The American Concrete Institute (ACI) is a leading authority and resource for the development and distribution of standards and technical references for individuals and organizations involved in concrete design, construction, and materials.

## Slide 13: Concrete Repair References
International Concrete Repair Institute
American Concrete Institute
American Society for Testing and Materials
References:
American Society for Testing and Materials (ASTM)
www.astm.org
Notes: The American Society for Testing and Materials (ASTM) is an international standards organization that develops and publishes voluntary consensus technical standards for a wide range of materials, products, systems, and services.

## Slide 14: Concrete Repair References
We will also refer to this Participant Guide throughout the course.
Let’s get started!
Notes: Finally, you should have all received a handout “Participant Guide” that we will refer to throughout the course.
Let’s get started.

## Slide 15: Concrete Basics

## Slide 16: Concrete Basics
In this lesson we will cover…
  What makes up concrete
  How reinforced concrete combats compression and tension forces
  Why repairs fail
  How to increase the likelihood of planning a lasting repair
Notes: Review lesson objectives.

## Slide 17: Make-up of Concrete
Cement:
A binder that works in concrete to hold aggregate together
Aggregate:
The gravel or sand that gives the concrete mass (can vary in size)
Water:
Activates the cement to hold it all together
10-15%
60-75%
15-20%
+
+
The make-up or “recipe” of concrete can change based on desired outcomes, therefore many variations are possible.
For example, one could:
Increase water
Include additives (admixtures)
Use different sized aggregate
Concrete is a composite material of cement, aggregate, and water.
Notes: Before we begin discussing how to effectively evaluate and repair damaged concrete, it is important to understand how reinforced concrete works.
Concrete is a composite material comprised of three main elements: the cement, the aggregate, and the water.
Cement only accounts for about ten-to-fifteen percent of the total composite, depending on the application. The remaining bulk is aggregate. The water activates the cement as the binder and hydrates the concrete.
Sometimes these ratios change. There are a limitless number of “recipes” for concrete. Choosing the right one depends on a variety of factors. We will cover how to choose the best repair materials and methods in this course.
----------------------------------------
Quiz Note
This slide features information that will be found on the post-course knowledge assessment.
True or false: In its most basic form, concrete is comprised of water, cement, and aggregate.
True
False

## Slide 18: How Concrete Reacts Under Loading
Compression
Tension
Compression
4000 PSI
Tension
400 PSI
Concrete without reinforcement is strong in compression, but weak in tension.
Shortens
Lengthens
What can be done to combat this?
Notes: Concrete is strong in compression–this is one of the reasons it is used in columns and areas that carry heavy loads like roadways and flooring. However, it is weak in tension.
In this image, we can see that when a vertical slab of concrete is subjected to vertical gravity loads, it naturally wants to bow out of plane. The top of the concrete slab is experiencing compression and will shorten, but its integrity will not be compromised. When we examine the bottom of the slab, we can see it is experiencing tension. It has began to crack along the point that is most impacted by the gravity load.
What can be done to combat this?
----------------------------------------
Quiz Note
This slide features information that will be found on the post-course knowledge assessment.
True or false: Concrete is strong in tension, but weak in compression.
True
False

## Slide 19
How Reinforced Concrete Acts Under Loading
Shortens
Lengthens
Compression
Tension
Concrete carries COMPRESSION loads
Steel carries TENSION loads
Concrete with reinforcement is strong in compression and tension.
Notes: Added reinforcement, such as a steel reinforcing bar (or rebar, as it is called in the field), along the bottom of the slab, can carry the tension load. The top of the slab will still be carrying the compression load, but since concrete is strong in compression, this part of the beam will not require reinforcement.
----------------------------------------
Quiz Note
This slide features information that will be found on the post-course knowledge assessment.
True or false: Concrete is strong in tension, but weak in compression.
True
False

## Slide 20: Make-up of Reinforced Concrete
Reinforced concrete is a composite
Concrete carries compression strength
Reinforcing bar carries tension strength
Together, the reinforcing bar and the concrete create a composite that is strong in compression AND tension.
Notes: Reinforced concrete is considered a composite material. A composite material refers to materials made up from two or more materials with significantly different properties that, when combined, produce a material with characteristics different from the individual components.
Since this composite of steel reinforcing bar and concrete is strong in both compression and tension forces, it is ideal for a number of structural applications.

## Slide 21: Where is concrete used?
Because reinforced concrete is strong in both compression and tension, it is the most widely used building material in the world.
Concrete can be used for:
  Roadways
  Bridges
  Columns
  Foundations
  Parking structures
  Barriers
  …and many more applications
Notes: Concrete is one of the most widely used building materials because of its flexibility of design and versatility. It can be used in roadways, bridges, flooring, columns, and parking structures in addition to numerous other applications.

## Slide 22: Concrete Lifespan and Failure Modes
If well designed and regularly maintained, concrete could last up to 50 years
… but many factors decrease this lifespan, such as:
Corrosion of Embedded Rebar
Disintegration Mechanisms
  Exposure to aggressive chemicals
  Freeze-thaw disintegration cycles
  Alkali-aggregate reactions
  Sulfate attacks
  Erosion by cavitation or abrasion
Moisture/Thermal Effects
Load Effects
Unanticipated Disasters
  Tornados, earthquakes, hurricanes etc.
Improper Design or Construction
In this image, the concrete failed because the embedded metal reinforcing bar corroded
For more information on why concrete deteriorates, refer to our Deterioration course.
Notes: It is impossible to determine the lifespan of any placed concrete because there are so many factors that affect concrete’s performance. While some concrete can last for up to 50 years, other concrete may be subjected to damaging conditions and may only last a year or two before it begins to fail.
Factors that may lead to concrete deterioration include embedded rebar corrosion, disintegration mechanisms (such as aggressive chemicals), freeze-thaw cycles, abrasion, moisture effects, thermal effects, heavy loads the structure was not intended to carry, unanticipated disasters, or improper design or construction.
It can also be a combination of these things!
For more information on why concrete deteriorates, let participants know that there is also a “concrete deterioration” course that we offer as an online course.

## Slide 23: What is the most common repair failure?
Chart: Most Common Repair Failures
| Corrosion | Cracking | Debonding | AAR | Other
Series 1 | 22 | 30 | 24 | 4 | 15
Repair failures are usually caused by:
the incorrect diagnosis of the original cause of the deterioration
the incorrect design of the repair or method of application
incorrect selection of material
poor workmanship
CON REP NET Network Newsletter No. 3." CON REP NET. N.p., May 2004. Web. June 2015.
All of these issues could have been prevented if the specifier or installer had known better!
Why do concrete repairs fail?
Alkali-Aggregate Reaction
Notes: As you can see from this chart, cracking is the most common mode of failure in repaired concrete. It is also usually the first indicator of a deeper problem. Cracking may be an indicator of corrosion, alkali-aggregate reaction, freeze-thaw disintegration, drying shrinkage, abrasion, or a variety of other issues.
There are a variety of reasons why concrete fails. Here we can see a few of the most common causes, including the incorrect diagnosis of the original cause of the deterioration, the incorrect design of the repair and method of application, incorrect selection of material or poor workmanship.
All of these causes of failure are fixable! Proper education can prevent these types of failures from happening.
----------------------------------------
Quiz Note
This slide features information that will be found on the post-course knowledge assessment.
Which of the following is the most common way a repair fails?
Debonding
Alkali-Aggregate Reaction
Cracking

## Slide 24: Repairing Concrete
The best way to fix deteriorated concrete is to completely start over.
But that’s not always feasible.
In this course, we’re going to look at the ways to repair existing concrete structures in order to prolong the service life.

## Slide 25: How effective are repairs?
HALF
of all concrete repairs fail within the five years of being placed.
Why is this?
The main reason repairs fail is because they are designed without assessing the cause of the damage.
Notes: Ask the audience: What percentage of concrete repairs are effective after 5 years?
Once a few people respond, reveal the correct answer.
Experts estimate that half of all concrete repairs fail within the first five years.
When you consider 1.) that repair materials are often stronger than the substrate they are replacing and 2.) that new concrete could last up to 50 years if properly placed and treated, it is obvious that repairs are not being effectively executed. As we just saw, many times, a repair is conducted without understanding what caused the concrete failure/deterioration in the first place!
Let’s look at an example.

## Slide 26: Example: Cracking
Corroding reinforcing steel bar
What caused this crack?
Cracks can be caused by a variety of issues, how we repair them depends on what caused the damage.
In this case, the crack was caused by the corrosion of the reinforcing bar.
Notes: Here we can see that this concrete was cracked, which is one of the most common concrete repair failure methods. Cracks can be caused by a variety of issues, ranging from impact loads, to corrosion of the embedded metal rebar.

## Slide 27: Example: Cracking
Corroding reinforcing steel bar
Cracks provide access for surface-introduced chlorides
Cracking and spalling of the concrete
What does “corrosion of reinforcing bar” mean?
Carbonation changes the pH of the concrete and therefore removes the passivity layer that protected the concrete.
Notes: When a reinforcing bar corrodes, the build-up of rust increases the volume of the bar. The concrete above the reinforcing bar cannot accommodate for this volume change so it cracks and eventually spalls off.
In this example, this concrete cracked because chlorides seeped through the concrete, reached the reinforcing bar, and corrosion of the steel rebar began.
The process of carbonation changed the pH of the concrete (from a more to a less alkaline environment) due to the interaction of water, atmospheric carbon dioxide, and the calcium hydroxide in the cement paste. Calcium hydroxide is a bi-product of the cement hydration process.
The lower pH causes the passivity layer around the rebar to diminish, which makes the concrete more conducive to setting up a corrosion cell.

## Slide 28: What does cracking show?
Cracks in concrete should be like a smoke alarm—an indicator of a larger problem that needs to be investigated.
“Something is wrong here! Investigate the issue!”
If the crack in the previous slide was not addressed, more serious spalling could occur and the concrete could reach its ultimate capacity and fail.
Notes: Concrete fails when it reaches its ultimate capacity, but this may not happen all at once. Often the first sign of distress in a concrete structure is tension cracks.
Think of these tension cracks as “smoke alarms” as they are often the first indicators that something is wrong and needs to be looked into.
If the crack in the previous slide was not addressed, more serious spalling could occur and the concrete could reach its ultimate capacity and fail.

## Slide 29: Example: Cracking
Because the underlying issue was not addressed…
What would happen if we just filled this crack with an epoxy resin?
eventually, the repair will fail.
Notes: However, let’s say the person designing this repair did not investigate this issue. Instead of addressing the underlying corrosion of the reinforcing bar, they simply filled the crack with an epoxy resin, using a gravity-feed method.
Ask the audience what they think will happen. After you have given the audience a change to answer, proceed.
The reinforcing bar will keep corroding. The repair will fail because the cause of the problem was not addressed.
In fact, because the repair material is often stronger that the substrate, more cracks would form parallel to the area repaired with epoxy. This creates more opportunities for chlorides or disintegrating agents to enter the concrete and access the reinforcing bar. The repair will have to be executed again, only this time, the surrounding concrete will need to be completely removed, the rebar will need to be cleaned, and new concrete will have to be laid. Although this is a more expensive repair than the epoxy repair first used, the epoxy repair was not a solution to the problem. The first repair was an entire waste. If the larger repair was done first, it would have provided a lasting solution and been altogether less expensive.

## Slide 30: The Process
Assess
1
Plan
2
Prepare
3
Execute
4
It is essential to assess the underlying cause of the damage before you plan your repair.
In this course, we will cover the factors that should be considered at each step along the way in order to create a successful repair.
Notes: It is essential to assess the underlying cause of the damage before planning a repair.
During a concrete repair, follow the four step process: Assess, Plan, Prepare, and Execute.
In this course, we will cover the factors that should be considered at each step along the way in order to create a successful, lasting repair.

## Slide 31: Assessing and Planning a Repair

## Slide 32: Assessing and Planning a Repair
In this lesson we will cover…
  How to conduct a visual inspection.
  How to assess if concrete is delaminated.
  Other requirements that should be considered prior to planning the repair.
Notes: Review lesson objectives.

## Slide 33: How do we assess the condition?
Assess
Sometimes the cause of the concrete failure is obvious
…sometimes it’s not.
The Project Engineer should conduct a thorough assessment of the damaged area in order to plan the best repair.
Notes: In order to identify the problem, we first have to assess the area that needs to be repaired.
In some cases, the course of the concrete failure is obvious, such as fire damage. In other instances, the cause may only be determined after a careful evaluation.

## Slide 34: Concrete Assessment: Visual Inspection
Assess
In order to identify the problem, first assess the area that needs to be repaired.
Visual Inspection
  Note observable characteristics of failure (moving or non-moving cracks?)
  Note environment
  Note potential loads
  Note extent of damage
  Take pictures of damage for reference
Notes: First, conduct a visual inspection. Note if there are any spalls, cracks, discoloration, or any other observable characteristics of failed concrete. If there are cracks, determine if they are moving or non-moving, this will dictate which repair method to use. Also, observe the environment. If the repair is outside, what typical weathering elements is this structure subject to? Is the area damp? Is it subject to heavy loads or traffic? Does the failure seem to be localized to the surface or does it go deeper?

## Slide 35: Concrete Assessment: Collection of Data
Assess
Collect any existing data that may aid in the assessment of the existing structure.
Collection of Data
  Original construction documents and drawings
  Soil reports
  Maintenance records
  Inspection reports
  Quality control documents
Refer to ACI 546R-14 Guide to Concrete Repair for more examples of types of data that may be valuable to refer to when assessing the damaged area.
Notes: Next, collect all data that pertains to the structure. This step in the process will include, but is not limited to, reviewing the original construction documents and drawings, soil reports, maintenance reports, inspection reports and documents related to the quality control of the materials, and mixture ratios used in the original placement.

## Slide 36: Concrete Assessment: Visual Inspection
  Year built?
  Areas of distress?
  Cracks?
  Scaling?
  Exposed rebar?
  Environment?
  Loading conditions?
  Foundation conditions?
  Type of aggregate?
  Mixture proportions?
Assess
A Concrete Condition Checklist is a useful tool when performing an assessment.
For a more detailed concrete condition survey, refer to
ACI 201.1R-08 Guide for Conducting a Visual Inspection of Concrete in Service.
Notes: Direct participants to page 2 in their Participant Guide that should have been passed out at the beginning of the class.
This checklist can be useful for the Project Engineer when conducting a visual concrete assessment.

## Slide 37: Concrete Assessment: Testing and Examination
Assess
First, conduct a non-destructive evaluation (NDE) to check for delamination.
If you hear a “pinging” sound, this means the concrete is delaminated.
Hammer Sounding
Image from ACI RAP-4
Chain Dragging
Image from ACI RAP-7
For more information on other methods, refer to
ACI 228.2R-13 Report on Nondestructive Test Methods for Evaluation of Concrete in Structures
ICRI 210.4 Guide for Nondestructive Evaluation (NDE)
Notes: First, conduct a non-destructive surface evaluation to check for concrete delamination. Two of the most popular methods for doing so are hammer sounding and chain dragging. In these methods, you will hear a “pinging sound” if the concrete is delaminated.
However, this is not the only method to test for concrete delamination. Other methods for identifying delaminated concrete include:
Impact echo-testing (ASTM C1383)
Ground-penetrating radar (GPR) (ASTM D4788)
Infrared thermography typically accompanied by sounding by hammer tapping, chain dragging or impulse response.
For more information, refer to ACI 228.2R-13 Report on Nondestructive Test Methods for Evaluation of Concrete in Structures and ICRI 210.4-2009 Guideline for Nondestructive Evaluation Methods for Condition Assessment, Repair, and Performance Monitoring of Concrete Structures.

## Slide 38: Concrete Assessment: Testing and Examination
Assess
Depending on the outcome of the sounding, the planning of the repair will differ.
After sounding the area, was delamination found?
Yes
No
Delaminated concrete needs to be removed and replaced.
Concrete does not need to be removed and replaced.
Cracks caused by abrasion, overloading, shrinkage, or other non-corrosive means may not be accompanied by delaminated concrete.
Notes: Based on the findings of the sounding (or other delaminated concrete location means) a decision will need to be made. If the concrete is sounded and no delamination is present, the concrete does not have to be removed and replaced since delaminated concrete has already lost significant strength and will no longer perform as expected. Other repair methods can be considered depending on the nature of the damage. This being said, one still needs to determine the cause of the damage before planning the repair.
Cracks caused by abrasion, overloading, shrinkage, or other non-corrosive means may not be accompanied by delaminated concrete. For example, if light honeycombing occurred without the presence of delamination, the surface could be re-profiled and new material could be added without major concrete removal.
If delamination was discovered, the deteriorated concrete will need to be removed, undercut, and replaced.

## Slide 39: Decision Point Continued
“But if no delaminated concrete is found, why do we need to fix the crack?”
  Cracks make it easier for deteriorating agents to access the concrete or reinforcing bar.
ALWAYS address the issue as soon as possible. This will save time, money, and labor in the long run.
REMEMBER:
Notes: Some may think that cracks that are not associated with delaminated concrete do not need to be filled and are only an aesthetic concern. This is a false assumption.
As covered previously, cracks make it easier for deteriorating agents to access the concrete or reinforcing bar. If cracks are not sealed, these deteriorating agents (such as moisture, sulfates, de-icing salts, salt water, and other corrosive agents) can easily access the concrete and/or reinforcing bar which can lead to corrosion, alkali-aggregate reactions, or freeze-thaw deterioration. Not only are these situation more devastating to the make-up of the concrete, they are much more costly and labor intensive to repair.
Fixing the situation as soon as it arises is always the best way to save time and money in the long run.

## Slide 40: Concrete Assessment: Testing and Examination
Assess
Based on the outcome of the sounding and the other evidence collected so far, there should be enough information to determine what types of tests (if any) are needed.
Testing and Examination
  Chloride and sulfate content test
  Alkalinity test
  Depth of carbonation test
  Crack movement test
Seen here is the “Tensile Pull-Off Tests to Evaluate Bond of Concrete Surface Materials” outlined in ICRI No. 210.3. Refer to this guidelines for more information on how to conduct this test.
Notes: Based on the outcome of the sounding and other evidence collected so far in the visual and collection of data phases, there should be enough information to recognize which types of tests would be useful for further evaluation.
These tests can include chloride and sulfate content testing, alkalinity testing, depth of carbonation testing, and testing if cracks are moving or non-moving. The results of these test will help determine which repair material and placement method is appropriate for the repair at hand.
There are many different methods for testing the damaged substrate. Refer to ICRI Technical Guidelines for more information on how to conduct various tests for evaluating existing concrete substrate.

## Slide 41: Identify the Cause
What caused the deterioration?
Carbonation
Fire
Overloading
Environmental pollution
Earthquake
Frost
Inadequate coverage of reinforcement
Corrosion of reinforcement
High water content
Aging
Plants or microorganisms
Oils
Acids
Poor workmanship
Deicing salts
Faulty design
Acids
Often it is not just one thing, but rather a
combination of these factors that causes deterioration.
Notes: After the assessment is completed, the Project Engineer should have a pretty good idea of what caused the failure.
Concrete deterioration is often not just caused by one thing. It is usually caused by a combination of these factors.

## Slide 42
Course Scenario
Throughout this course, we will apply what we’ve learned to a concrete repair scenario.
We will build upon the information after each lesson.
Let’s get started!

## Slide 43
It's November in Maryland. The job at hand is on the top level of a parking garage.
Let’s say the Project Engineer is conducting a visual repair. What are some things he/she should note?
Moderate, patterned cracking with some spalling.
After sounding, delaminated concrete is found.
(possibly corrosion of embedded metal reinforcement?)
Currently snowy climate, but some sun
(possibly freeze/thaw?)
Slipping caution (possibly de-icing salts?)
Notes: Let’s examine some of the things that are going on in this picture.
First, we should notice that moderate, patterned cracking with some spalling has occurred. When cracking occurs in lines like this, this is usually a good indicator that the reinforcing bar has experienced some kind of corrosion since there are cracks directly above where the rebar may be. Be sure to look at the original construction plans and see if the cracks line up with where the rebar was placed.
Next look at the climate. Since it is November in Maryland, there is some snow, but also some sun peeking through. Since this is the top level of the parking garage, the surface is mostly likely in direct sunlight and is directly in contact with snow. Perhaps these cracks were caused by freeze/thaw cycles.
Finally, we can see that there is sign that warns against slipping on the stairs. Given that it is also snowing, perhaps icy ground is an issue in this area. Be sure to make a note to ask the owner if de-icing salts are used.

## Slide 44
When going through the construction documents and data, the Project Engineer finds a few things he is curious about.
It seems a repair was done on this structure only a few years ago...

## Slide 45
The Stakeholder
“Do you use de-icing salts to prevent skidding?”
“We use them a lot, otherwise cars skid all over the place.”
“When was the concrete last serviced?”
“I’m not sure. Let me check and get back to you.”
“Is this area subject to heavy loading?”
“Not really, since it’s the top level of the garage, it doesn’t get much use until we’re overloaded with holiday shoppers.”
Let’s have the Project Engineer ask the Owner/Stakeholder a few questions based on what he’s seen.
The Project Engineer

## Slide 46
He suspects that de-icing salts may be the cause.
A review of past records show that none of the previous repairs did anything to protect the reinforcing bar.
De-icing salts (chlorides) accelerate the rate of corrosion by breaking down the initial protective layer of iron oxide that forms on the reinforcing steel when concrete is first placed.
“We need to conduct a pH test and a chloride test on the concrete using ASTM D4262 and ASTM C1152, respectively, as reference standards.”

## Slide 47
Based on these test results and general observations, the Project Engineer concludes that de-icing salts caused corrosion of the embedded metal rebar which led to patterned cracking.
Result of the pH test:
Low pH
Result of the chloride test
High amounts of chlorides detected

## Slide 48
Discussion Question:
Were there other things that could have accelerated the deterioration?
Notes: Lead a class discussion about other factors that may have present in this repair that could have accelerated corrosion.
Some ideas to discuss:
De-icing salts could have absorbed water from melting snow.
Cracks could have been caused by freeze-thaw cycles and then the de-icing salts or other aggressive chlorides used the cracks as a pathway to access the rebar, causing corrosion.
Cars driving over already damaged surface could have contributed to surface abrasion.

## Slide 49
Can we fix the issue?
The Project Engineer
The Stakeholder
“Have you considered not using de-icing salts all together and rely simply on snow removal?”
“Snow removal alone won’t guarantee that cars won’t skid in my parking garage. Cars skidding and people slipping is a huge liability. I can’t change.”
The Project Engineer determines that he needs to design a repair that adequately protects the reinforcing bar so that this issue does not continue to happen.
Notes: Since the Project Engineer can’t change the situation (the Owner wants to continue to use the harsh de-icing salts), the repair will be need to be designed to decrease the likelihood of this issue reoccurring.

## Slide 50: Determining the Scope of the Repair
Owner Requirements
Service Conditions
Application Conditions
Establishing Repair Requirements:
Certain requirements will also affect how the repair is planned.
These requirements include:
  Owner Requirements
  Application Conditions
  Service Conditions
Notes: Direct participants to pages 4-6 in their participant guide for checklists taken from ICRI Guideline No. 320.2R-2009 Guide for Selecting and Specifying Materials for Repair of Concrete Surfaces.

## Slide 51: Determining the Scope of the Repair
Owner Requirements
Service Conditions
Application Conditions
Owner Requirements:
Do they want an aesthetically pleasing finish?
Are they concerned about a quick turn-around time?
What is their budget?
Notes: Because the owner funds the project, their requirements should especially be taken into account when planning the repair. In the example we just looked at, the Stakeholder had a few things he wanted that would affect how one would plan the repair.

## Slide 52: Determining the Scope of the Repair
Owner Requirements
Service Conditions
Application Conditions
Service Conditions:
What are the load carrying requirements?
Is the area exposed to atmospheric gases/chemicals?
What are the moisture and temperature conditions?
Notes: Service conditions refer to elements that the repair will be exposed to upon completion. Note that often the service conditions can often be determined during the visual inspection, collection of data, and testing phases of the evaluation.

## Slide 53: Determining the Scope of the Repair
Owner Requirements
Service Conditions
Application Conditions
Establishing Repair Requirements:
What is the temperature?
What will the wind velocity be at the time of the repair?
What is the geometric configuration of the damage?
What is the size and spacing of the reinforcing bar?
Notes: Application conditions refer to the physical limitations of the repair. Like service conditions, these requirements can be determined during the visual inspection, collection of data, and testing phases of the evaluation.

## Slide 54
The Stakeholder
“I want a clean finish so that my customers don’t have to drive over bumps but it doesn’t have to match perfectly.
Since it’s the holidays this parking lot often fills all the way up, I want it done as soon as possible.
I’m tired of doing this so often. I want a repair that will last at least another ten years but won’t cost that much.”
What Owner Requirements in our scenario would affect the repair material selected?
Clean finish
Matching not needed
Quick turn-around
Lasting repair
Low cost
Notes: Ask the audience identify which owner requirements would affect how the repair is planned.
After getting a few ideas, show the board with the list of notable requirements.

## Slide 55
What Service Conditions in our scenario would affect the repair material selected?
Exposure to de-icing salts
Exposure to UV rays
Exposure to moisture
Exposure to freezing temps
Notes: Ask the audience identify which service conditions would affect how the repair is planned.
After getting a few ideas, show the board with the list of notable requirements.

## Slide 56
What Application Conditions in our scenario would affect the repair material selected?
Some snow
Horizontal
30 degrees
Novice installer
Rebar 1”, spaced 1’
Notes: Ask the audience identify which application conditions would affect how the repair is planned.
After getting a few ideas, show the board with the list of notable requirements.

## Slide 57: Checkpoint Questions
Which of the following would be considered an owner requirements for a repair?
  Smooth surface texture desired
  Minimal UV exposure
  Temperature average high of 90°F
Notes: Time provided, ask these Check Your Knowledge Questions. You can hide questions that you do not want to ask prior to the presentation.

## Slide 58: Checkpoint Questions
Which of the following would be considered an owner requirements for a repair?
  Smooth surface texture desired
  Minimal UV exposure
  Temperature average high of 90°F
Owner requirements are limitations of the repair as dictated by the owner/stakeholder. These can include aesthetic elements, time constraints, hours of work, etc.

## Slide 59: Checkpoint Questions
Which of the following would be considered a service condition for a repair?
  Spacing of reinforcing bars 6” apart
  Minimal live loads
  Quick turn-around time
Notes: Time provided, ask these Check Your Knowledge Questions. You can hide questions that you do not want to ask prior to the presentation.

## Slide 60: Checkpoint Questions
Which of the following would be considered a service condition for a repair?
  Spacing of reinforcing bars 6” apart
  Minimal live loads
  Quick turn-around time
Service conditions refer to the elements the repair will be exposed to upon completion. The live loads the repaired structure will need to carry will dictate which types of materials should be used.

## Slide 61: Checkpoint Questions
Which of the following would be considered an application condition for a repair?
  Minimal live loads
  Repair thickness of 6” deep
  Low moisture condition
Notes: Time provided, ask these Check Your Knowledge Questions. You can hide questions that you do not want to ask prior to the presentation.

## Slide 62: Checkpoint Questions
Which of the following would be considered an application condition for a repair?
  Minimal live loads
  Repair thickness of 6” deep
  Low moisture condition
Application conditions refer to the physical limitations of the repair. The geometric configuration of the damage and other similar physical restraints will influence which materials and method of placement will be selected for a repair.

## Slide 63: Checkpoint Questions
If the crack is not associated with delaminated concrete, the surrounding concrete may remain and other repair methods can be considered.
  True
  False
Notes: Time provided, ask these Check Your Knowledge Questions. You can hide questions that you do not want to ask prior to the presentation.

## Slide 64: Checkpoint Questions
If the crack is not associated with delaminated concrete, the surrounding concrete may remain and other repair methods can be considered.
  True
  False
If a crack is not associated with delaminated, the surrounding crack may remain.
However, it is still important to assess the cause of the crack before planning the repair.

## Slide 65: Assessing and Planning a Repair
When conducting a concrete assessment be sure to visually inspect the concrete, review records, interview stakeholders, and conduct necessary testing to determine the cause.
To review:
Notes: Be sure to stop and ask the audience if there are any questions at this time.

## Slide 66: Repair Material Considerations

## Slide 67: Repair Material Considerations
In this lesson we will cover…
  How the properties of repair materials will affect the repair.
  How admixtures can be added to enhance certain properties.
  How to properly prepare a substrate to accept the repair material.
  How to select repair materials for different types of cracks.
Notes: Review lesson objectives.

## Slide 68: Planning the Repair
Is the repair structural or non-structural?
What are the owner requirements?
What is the environment like?
What is the desired turn-around time?
Is the crack delaminated?
Inadequate planning can be the major cause of concrete repair failures.
Planning a repair will require the Project Engineer to take many things into account.
Plan
Notes: Planning a repair will require the Project Engineer to take a variety of things into account.
Inadequate planning can be the major reason for concrete repair failures. If concrete fails mostly because of its environment and environmental factors were not taken into account when planning which materials and repair methods to use, the repair would not be successful.
In this section, we will look at what the Project Engineer will consider when selecting a repair material to increase the likelihood of a lasting repair. We will then move on to review the best way to apply these repair materials.

## Slide 69: Selection
Select repair materials
Select a method of placement
Review the physical properties and placement requirements for the repair material
Change the material or application method as needed.
1
2
3
4
This selection process order comes from ICRI 03731 Guide for the Selecting Application Methods for the Repair of Concrete Surfaces.
When selecting a suitable repair material and application method, the Project Engineer should proceed in the following sequence:
Notes: When selecting a suitable repair material and application method, the Project Engineer should proceed in the following sequence:
Select the repair material with the desirable material properties which best restore the integrity of the original design.
Select a method of placement which will successfully place the repair material into the prepared surface.
Review the physical properties and placement requirements for the repair material to ensure the constructability of the selected repair system.
Change the material or application method as needed to provide a constructible repair.
This means that the decision process is not always linear. Sometimes the Project Engineer will know the repair application first and then will have to find a repair material that is suitable for that application.
For the purposes of this course, however, we will begin by looking at the different types of concrete repair materials.

## Slide 70: Material Compatibility
Existing Substrate
Repair Material
Repair materials are inherently different than the existing substrate…
…but the goal is to match them as closely as possible.
Material incompatibility is a major cause of repair failures.
Notes: Selecting the correct material for an application is one of the most important parts of the repair process. Material incompatibility is a major cause of repair failures (ICRI 320.2R).
A repair will result in a composite material, comprised of the original concrete substrate, the bond area where the old and new material meet, and the repair material. The repair material will undoubtedly differ from the substrate in some way, but the goal is to match it as closely as possible so that it reacts similarly.
Compatibility is a balance of how the physical and chemical properties of the repair material and the substrate work together. Assessment of the proper repair materials must consider the behavior of the repair material in both cured and uncured states.

## Slide 71: Ideal Repair Materials
In the next slides, we’ll look at the different material properties of repair materials.
Certain material properties are essential for certain repairs. Remember that these properties should align with the repair requirements already determined by the checklists.

## Slide 72: Material Properties
Direct Tensile Strength
Direct Shear Strength
Slant Shear Strength
The bond strength of the repair material refers to how well it bonds with the existing substrate.
We’ll look at how bond strength can be evaluated in the next slides.
Please note that the information and images in the following slides are pulled from ICRI 320.2R-2009 Guide for Selecting and Specifying Materials for Repair of Concrete Surfaces.
For more information, please refer to this technical guideline.
Bond Strength
Notes: The bond strength of the repair material refers to how well it bonds with the existing substrate. This can be evaluated in many different directions that we will cover next.

## Slide 73: Material Properties – Bond Strength
Direct Tensile Strength
Direct Shear Strength
Slant Shear Strength
Direct tensile testing measures the tensile bond of the repair material and the substrate.
This is measured by dividing the load at failure with the cross sectional area of the core.
ASTM C1583
ICRI 210.3R-2013
Bond Strength
Notes: Direct tensile testing measures the tensile bond or tensile strength of surface repairs or overlays. These tests will expose the weakest material in the composite system. Tensile values are determined by dividing the load at failure by the cross sectional area of the core.
The following guidelines may be helpful when testing the direct tensile strength:
ASTM C1583 Standard Test Method of Tensile Strength of Concrete Surfaces
ICRI 210.3R-2013 Guide to Using In-Situ Tensile Pull-Off Test to Evaluate Bond of Concrete Surface Materials

## Slide 74: Material Properties – Bond Strength
Direct Tensile Strength
Direct Shear Strength
Slant Shear Strength
Pressure is applied in opposite directions and shear bond values are determined by dividing the recorded load at failure by the bond area.
Michigan DOT Shear Bond Test
Bond Strength
Notes: Direct shear testing measures the shear strength of the bond between the repair material and the substrate. Pressure is applied in opposite directions and shear bond values are determined by dividing the recorded load at failure by the bond area.
Michigan DOT Shear Bond Test method can be used to evaluate direct shear strength.

## Slide 75: Material Properties – Bond Strength
Direct Tensile Strength
Direct Shear Strength
Slant Shear Strength
Bond values are determined by dividing the load at failure by the elliptical bond area.
This value is typically reported by material suppliers.
ASTM C882
ASTM C1042
Bond Strength
Notes: Slant shear strength is often reported by material suppliers. Bond values are determined by dividing the load at failure by the elliptical bond area.
The following guidelines may be helpful when testing the slant shear strength:
ASTM C882 Standard Test Method for Bond Strength of Epoxy-Resin Systems Used with Concrete by Slant Shear
ASTM C1042 Standard Test Method for Bond Strength of Latex Systems Used with Concrete by Slant Shear (note that this standard was withdrawn in 2008 with no replacement)
----------------------------------------
Quiz Note
This slide features information that will be found on the post-course knowledge assessment.
True or false: A slant shear strength test measures a repair material's ability to resist bending.
True
False

## Slide 76: Material Properties
Drying Shrinkage
Coefficient of Thermal Expansion
Modulus of Elasticity
Dimensional behavior refers to how the repair material will behave over its service life.
We’ll look at how it can be evaluated in the next slides.
Please note that the information and images in the following slides are pulled from ICRI 320.2R-2009 Guide for Selecting and Specifying Materials for Repair of Concrete Surfaces.
For more information, please refer to this technical guideline.
Dimensional Behavior
Creep
Restrained Shrinkage
Notes: Dimensional behavior refers to how the repair material will behave over its service life. We will cover the different properties which influence dimensional behavior next.
Please note that the information and images in the following slides are pulled from ICRI 320.2R-2009 Guide for Selecting and Specifying Materials for Repair of Concrete Surfaces. For more information, please refer to this technical guideline.
----------------------------------------
Quiz Note
This slide features information that will be found on the post-course knowledge assessment.
Which material property refers to how the repair material will behave over the course of its service life?
Bond Strength
Dimensional Behavior
Mechanical Properties
Constructability

## Slide 77: Material Properties
Drying Shrinkage
Coefficient of Thermal Expansion
Modulus of Elasticity
Dimensional Behavior
Creep
Restrained Shrinkage
ASTM C157
Notes: In this image, we can see that repair materials that experience increased shrinkage are more likely to crack. Selecting a repair material with minimal drying shrinkage will increase the likelihood of a lasting repair.
ASTM C157 Standard Test Method for Length Change of Hardened Hydraulic-Cement Mortar and Concrete may be helpful when determining the drying shrinkage of a material.

## Slide 78: Material Properties
Drying Shrinkage
Coefficient of Thermal Expansion
Modulus of Elasticity
Dimensional Behavior
Creep
Restrained Shrinkage
ASTM C531
ASTM D696-08e1
Fig. 3-8 Thermal coefficient of expansion
The amount of expansion a particular material undergoes is known as the coefficient of thermal expansion.
Notes: All materials expand and contract with changes in temperature. The amount of expansion a particular material undergoes is known as the coefficient of thermal expansion.
Given a temperature change evenly distributed through the materials, the following stresses will occur according to the relationship of the thermal coefficients of the new and old materials. If the new and old material have equal coefficients of thermal expansion, then no stress occurs. However, if the new material has a higher thermal coefficient of expansion, the shear bond is stressed.
In this image, you can see that because the repair material has expanded, the bond area is experiencing stress.
The following guidelines may be helpful when determining the coefficient of thermal expansion:
ASTM C531 Standard Test Method for Linear Shrinkage and Coefficient of Thermal Expansion of Chemical-Resistant Mortars, Grouts, and Monolithic Surfacing, and Polymer Concretes
ASTM D696-08e1 Standard Test Method for Coefficient of Linear Thermal Expansion of Plastics

## Slide 79: Material Properties
Drying Shrinkage
Coefficient of Thermal Expansion
Modulus of Elasticity
Dimensional Behavior
Creep
Restrained Shrinkage
ASTM C469
ASTM C580
Modulus of elasticity (MOE) measures stiffness.
If the new material and the old substrate have the same MOE, no stress will occur. However, is one has more than the other, brittle material may become overstressed.
Fig. 3-9 Modulus of Elasticity
Notes: The modulus of elasticity measures stiffness. Materials with a higher modulus of elasticity (i.e., those that are stiffer) will deform less under a given load than materials with a lower modulus of elasticity. You can see here that if the new material has a lower modulus of elasticity, this will result on increased stress of the old material (on the right) and could lead to further damage.
The following guidelines may be helpful when determining the modulus of elasticity:
ASTM C469 Static Modulus of Elasticity
ASTM C580 Flexural Strength and Modulus of Elasticity for Chemical Resistant Mortars, Grouts and Monolithic Surfacings

## Slide 80: Material Properties
Drying Shrinkage
Coefficient of Thermal Expansion
Modulus of Elasticity
Basic creep refers to time-dependent deformation due to a sustained load.
Since the old material has already developed a stable creep volume, stresses may develop according to the amount of creep in the new material.
Dimensional Behavior
Creep
Restrained Shrinkage
Fig. 3-10: Tensile creep
ASTM C512
ASTM C1181
Notes: Basic creep refers to time-dependent deformation due to a sustained load. Drying creep refers to creep that is caused by the drying out of the material.
If the old material has already developed a stable creep volume, stresses will develop according to the amount of creep that occurs in the new material.
The following guidelines may be helpful when determining creep:
ASTM C512 Standard Test Method for Creep of Concrete in Compression
ASTM C1181 Standard Test Method of Compressive Creep of Chemical Resistant Polymer Machinery Grouts

## Slide 81: Material Properties
Drying Shrinkage
Coefficient of Thermal Expansion
Modulus of Elasticity
Restrained shrinkage occurs when a repair material that is bonded to a substrate begins to shrink and thus results in tension in the bond area.
Dimensional Behavior
Creep
Restrained Shrinkage
ASTM C1581
Notes: When shrinkage is restrained because the repair material is bonded to a substrate, this produces a tensile stress in the repair material. Because the concrete also creeps in response to sustained load, this and other factors can lead to an increased cracking potential.
In addition, drying shrinkage can cause the material to lose volume, reducing its ability to carry compressive loads.
ASTM C1581 Standard Test Method for Determining Age at Cracking and Induced Tensile Stress Characteristics of Mortar and Concrete Under Restrained Shrinkage can be used to assess how restrained shrinkage affects concrete’s strength.

## Slide 82: Material Properties
Permeability
Water Vapor Transmission
Resistance to Freezing and Thawing
Durability of a material refers to its ability to resist damaging service conditions. A durable repair will retain its original form, quality, and serviceability when exposed to its environment.
We’ll look at how certain properties can affect durability in the next slides.
Please note that the information and images in the following slides are pulled from ICRI 320.2R-2009 Guide for Selecting and Specifying Materials for Repair of Concrete Surfaces.
For more information, please refer to this technical guideline.
Durability
Resistance to Scaling
Sulfate Resistance
Alkai-Aggregate Reaction
Abrasion Resistance
Notes: Durability of a material refers to its ability to resist damaging service conditions. A durable repair will retain its original form, quality, and serviceability when exposed to its environment. We will cover the different material properties that can affect the durability of a repair next.
Please note that the information and images in the following slides are pulled from ICRI 320.2R-2009 Guide for Selecting and Specifying Materials for Repair of Concrete Surfaces. For more information, please refer to this technical guideline.

## Slide 83: Material Properties
Permeability
Permeability refers to the flow rate of a fluid (liquid or gas) into a porous solid such as concrete.
This property is a useful indicator of determining how much corrosion protection the repair material can provide.
Durability
Water Vapor Transmission
Resistance to Freezing and Thawing
Resistance to Scaling
Sulfate Resistance
Alkali-Aggregate Reaction
Abrasion Resistance
ASTM C1202
AASHTO T259
AASHTO T277
Notes: Permeability refers to the flow rate of a fluid (liquid or gas) into a porous solid such as concrete. This property is a useful indicator when determining how much corrosion protection a material can provide. If a repair material has a high permeability (meaning that liquid or gases can easily penetrate into the material) it may not provide as much corrosion resistance and therefore may be at a greater risk for deterioration.
ASTM C1202 Standard Test Method for Electrical Indication of Concrete’s Ability to Resist Chloride Ion Penetration may be helpful to refer to when determining the permeability of a repair material.
The American Association of State Highway and Transportation Officials (AASHTO) have also created several test method guidelines to evaluate material permeability:
AASHTO T259 Resistance of Concrete to Chloride Ion Penetration
AASHTO T277 Rapid Determination of the Chloride Permeability of Concrete

## Slide 84: Material Properties
Water Vapor Transmission
Durability
Permeability
Resistance to Freezing and Thawing
Resistance to Scaling
Sulfate Resistance
Alkali-Aggregate Reaction
Abrasion Resistance
ASTM E96
Water vapor transmission refers to the flow of water vapor through a material.
Notes: Water vapor transmission is the flow of water vapor through a material. If the repair material is less permeable than the substrate, the water vapor transmitted through the substrate may be trapped where the two substances meet. Because moisture is trapped at the bond area, this could result in freeze-thaw damage.
ASTM E96 Standard Test Method for Water Vapor Transmission of Materials may be helpful when determining the amount of water vapor transmitted in a material.

## Slide 85: Material Properties
Resistance to Freezing and Thawing
Freezing and thawing deterioration occurs when saturated concrete freezes and expands and thus failure occurs.
This is particularly damaging when concrete undergoes this cycle several times.
Durability
Permeability
Water Vapor Transmission
Resistance to Scaling
Sulfate Resistance
Alkali-Aggregate Reaction
Abrasion Resistance
ASTM C666
Notes: Concrete can become damaged when water that is in the concrete expands when it freezes and then contracts once the water thaws. Materials that resist this cycle may yield more lasting repairs.
ASTM C666 Standard Test Method for Resistance of Concrete to Rapid Freezing and Thawing outlines a test to evaluate a materials ability to resist freeze-thaw cycles.

## Slide 86: Material Properties
Scaling is the flaking or peeling away of hardened concrete.
Durability
Resistance to Scaling
Permeability
Water Vapor Transmission
Resistance to Freezing and Thawing
Sulfate Resistance
Alkali-Aggregate Reaction
Abrasion Resistance
ASTM C672
Notes: Scaling is the flaking or peeling away of hardened concrete or mortar. Most frequently, scaling is caused when harsh de-icing salts are introduced to the surface. Materials that resist this characteristic are more likely to result in lasting repairs.
ASTM C672 Standard Test Method for Scaling Resistance of Concrete Surfaces Exposed to Deicing Chemicals is widely accepted as a good indicator of the materials ability to resist scaling from de-icing chemicals.

## Slide 87: Material Properties
Sulfate attacks causes the chemical decomposition of certain binder compounds in hydrated cement paste.
Durability
Sulfate Resistance
Permeability
Water Vapor Transmission
Resistance to Freezing and Thawing
Resistance to Scaling
Alkali-Aggregate Reaction
Abrasion Resistance
ASTM C1012
Notes: Sulfate attacks causes the chemical decomposition of certain binder compounds in hydrated cement paste. This can lead to concrete deterioration. Sulfates can come from the decay of organic matter and therefore naturally occur in some soils. Sulfates can also come from non-organic means, such as from wastewater treatment plants. Sulfate resistance should be considered in applications where sulfate interaction is anticipated.
This graph shows the amount of sulfate content that may be present in water or soil in various sulfate attack severities.
ASTM C1012 Standard Test Method for Length Change of Hydraulic-Cement Mortars Exposed to Sulfate Solutions has classified sulfate attacks into three categories: moderate, severe, and very severe. Refer to this reference standard as needed.

## Slide 88: Material Properties
An alkali-aggregate reaction (AAR) is a chemical reaction that occurs in the concrete between alkalies (sodium or potassium) and certain constitutes of the concrete’s aggregate.
Durability
Alkali-Aggregate Reaction
Permeability
Water Vapor Transmission
Resistance to Freezing and Thawing
Resistance to Scaling
Sulfate Resistance
Abrasion Resistance
ASTM C227, ASTM C289, ASTM C295
Notes: An alkali-aggregate reaction (AAR) is a chemical reaction that occurs in the concrete between alkalies (sodium or potassium) and certain constitutes of the concrete’s aggregate. The bi-products of this reaction often causes expansion and thus results in the cracking of the concrete in service.
The ASTM has several guidelines that may be helpful when determining the AAR potential in concrete:
ASTM C227 Standard Test Method for Potential Alkali Reactivity of Cement-Aggregate Combinations (Mortar Bar Method)
ASTM C289 Standard Test Method for Potential Alkali-Silica Reactivity of Aggregates (Chemical Method)
ASTM C295 Standard Guide for Petrographic Examination of Aggregates for Concrete

## Slide 89: Material Properties
Abrasion refers to when a surface is worn away by rubbing or friction.
Durability
Abrasion Resistance
Permeability
Water Vapor Transmission
Resistance to Freezing and Thawing
Resistance to Scaling
Sulfate Resistance
Alkali-Aggregate Reaction
ASTM C418, ASTM C779, ASTM 944, ASTM C1138
Notes: Abrasion refers to when a surface is worn away by rubbing or friction. Factors that influence abrasion resistance include the amount and quality of the aggregate, the material’s compressive strength, the mixture proportions, the type of material, and the finishing procedures.
The following ASTM test methods provide guidelines for procedures to determine the abrasion resistance of a repair material:
ASTM C418 Standard Test Method for Abrasion Resistance of Concrete by Sandblasting
ASTM C779 Standard Test Method for Abrasion Resistance of Horizontal Concrete Surfaces
ASTM C944 Standard Test Method for Abrasion Resistance of Concrete or Mortar Surfaces by the Rotating-Cutter Method
ASTM C1138 Standard Test Method for Abrasion Resistance of Concrete (Underwater Method)

## Slide 90: Material Properties
Tensile Strength
Flexural Strength
Compressive Strength
Repair materials should be able to absorb and resist stress in the structure.
We’ll look at how it can be evaluated in the next slides.
Please note that the information and images in the following slides are pulled from ICRI 320.2R-2009 Guide for Selecting and Specifying Materials for Repair of Concrete Surfaces.
For more information, please refer to this technical guideline.
Mechanical Properties
Notes: In addition to all the properties already covered, ideally, the repair materials will also posses mechanical properties that can carry and transfer loads similar to the concrete which is being repaired. These repair materials should also be able to absorb and resist stress caused by restrained volume changes.
Please note that the information and images in the following slides are pulled from ICRI 320.2R-2009 Guide for Selecting and Specifying Materials for Repair of Concrete Surfaces. For more information, please refer to this technical guideline.

## Slide 91: Material Properties
Tensile Strength
Flexural Strength
Compressive Strength
A material’s tensile strength is an indication of its ability to withstand tensile stress.
Mechanical Properties
ASTM C190, ASTM C496
Notes: A material’s tensile strength is an indication of its ability to withstand tensile stress. There are two standard tests for evaluating tensile strength in concrete repair materials, as seen here.
Two of the most common ways to measure tensile strength are outlined in the following guidelines:
ASTM C190 Method of Test for Tensile Strength of Hydraulic Cement Mortars (Note that even though this guideline was withdrawn by ASTM in 1990, the procedure is still used for lack of an alternative direct tensile test.)
ASTM C496 Standard Test Method for Splitting Tensile Strength of Cylindrical Concrete Specimens
----------------------------------------
Quiz Note
This slide features information that will be found on the post-course knowledge assessment.
Which of the following material properties is considered a mechanical (strength) property?
Tensile strength
Constructability
Shrinkage

## Slide 92: Material Properties
Tensile Strength
Flexural Strength
Compressive Strength
Flexural strength measures a repair material’s ability to resist bending.
Mechanical Properties
ASTM C78, ASTM C348, ASTM C42
Notes: Flexural strength measures a repair material’s ability to resist bending.
The following ASTM guidelines can be used to determine a repair material’s flexural strength:
ASTM C78 Standard Test Method for Flexural Strength of Concrete (Using Simple Beam With Third-Point Loading)
ASTM C348 Standard Test Method for Flexural Strength of Hydraulic Cement Mortars
ASTM C42 Standard Test Method for Obtaining and Testing Drilled Cored and Sawed Beams of Concrete

## Slide 93: Material Properties
Tensile Strength
Flexural Strength
Compressive Strength
The compressive strength of a repair material measures its ability to carry compressive loads.
Differences in compressive strength usually indicate differences in modulus of elasticity (stiffness) as well.
Mechanical Properties
ASTM C109, ASTM C39, ASTM C42
Notes: The compressive strength of a repair material measures its ability to carry compressive loads. Differences in compressive strength usually indicate differences in modulus of elasticity (stiffness) as well.
High compressive strengths are frequently achieved by increasing the cement content in the mixture. Possible negative effects of higher cement content include increased drying shrinkage and excessive temperature rise.
The following ASTM guidelines can be used to determine a repair material’s compressive strength:
ASTM C109 Standard Test Method for Compressive Strength of Hydraulic Cement Mortars
ASTM C39 Standard Test Method for Compressive Strength of Cylindrical Concrete Specimens
ASTM C42 Standard Test Method for Obtaining and Testing Drilled Cores and Sawed Beams of Concrete

## Slide 94: Material Properties
Flow Characteristics
Rate of Strength Gain
Exothermic
Finally, constructability properties refer to the properties of the repair materials during an early age and dictate how they will be placed.
We’ll look at how certain properties can affect durability in the next slides.
Please note that the information and images in the following slides are pulled from ICRI 320.2R-2009 Guide for Selecting and Specifying Materials for Repair of Concrete Surfaces.
For more information, please refer to this technical guideline.
Constructability
Hot and Cold Weather Applications
Working Time
Other Considerations
Notes: Finally, constructability properties refer to the properties of the repair materials during an early age and dictate how they will be placed. It’s important to note that while some of these properties make the repair material easier to place, they may negatively affect other material properties.
Please note that the information and images in the following slides are pulled from ICRI 320.2R-2009 Guide for Selecting and Specifying Materials for Repair of Concrete Surfaces. For more information, please refer to this technical guideline.

## Slide 95: Material Properties
Flow Characteristics
Rate of Strength Gain
Exothermic
Flow characteristics refer to how well the repair material penetrates and consolidated into the repair cavity.
Constructability
Hot and Cold Weather Applications
Working Time
Other Considerations
ASTM C939
Do NOT add more water to increase flowability, this will increase the potential drying shrinkage.
Notes: Flow characteristics refer to how well the repair material penetrates and consolidated into the repair cavity. With certain placement techniques that we will cover later in the course (e.g., form and pump, cast-in-place, or preplaced aggregate), good flowability is critical for a successful repair. Sometimes in the field, more water is added to increase the flowability of the material. This should be avoided as more water increases potential drying shrinkage which can weaken the integrity of the repair material.
Preplaced aggregate applications will require flowability to be measured with a flow cone as outlined in ASTM C939 Standard Test Method for Flow of Grout for Preplaced-Aggregate Concrete.

## Slide 96: Material Properties
Flow Characteristics
Rate of Strength Gain
Exothermic
Rate of strength gain refers to how quickly the concrete gains its compressive strength.
Constructability
Hot and Cold Weather Applications
Working Time
Other Considerations
Faster strength gain
Slower strength gain
Notes: This property refers to how quickly the concrete gains its compressive strength. It’s important to note that the rate of strength gain is also highly dependent on the temperature. Insufficient strength gain prior to use may result in damage to the repair material or bond area. The rate of strength gain is also highly dependent upon the temperature of the cure. Higher temperatures will often result in a faster strength gain and lower temperatures will result in a lower strength gain.
To accurately measure in-situ strength is it best to match cure specimens at temperatures similar to those which exist in the in-situ repair material.

## Slide 97: Material Properties
Flow Characteristics
Rate of Strength Gain
Exothermic
An exothermic reaction (heat) occurs when water is added to cement. Thermal cracking typically occurs when the concrete undergoes tensile stress from the restraint of volume changes which occur as the material cools and cures.
Constructability
Hot and Cold Weather Applications
Working Time
Other Considerations
ASTM C150, ASTM C595
Heat is measured in
Notes: An exothermic reaction occurs when water is added to cement. This results in heat that can be measured in calories per unit weight of cement (cal/g). High early strength cements tend to achieve more rapid release of heat since they are setting more quickly. In thick section repair applications, failure to provide proper dissipation may result in thermal cracking.
Thermal cracking typically occurs when the concrete undergoes tensile stress from the restraint of volume changes which occur as the material cools and cures. To combat this, it’s essential to restrict the amount of thermal heat generated.
Refer to the following guidelines for more information on how to control the amount of heat generated by thermal reactions:
ASTM C150 Standard Specification for Portland Cement
ASTM C595 Standard Specification for Blended Hydraulic Cements

## Slide 98: Material Properties
Flow Characteristics
Rate of Strength Gain
Exothermic
Both hot and cold weather applications can result in poor bond between the substrate and repair material.
Constructability
Hot and Cold Weather Applications
Working Time
Other Considerations
ACI 305, ACI 306
Notes: Hot weather’s adverse effects include plastic shrinkage cracking, drying shrinkage cracking, and poor surfaces finishes due to rapid setting.
Cold weather’s adverse effects include freezing of the repair material and subsequent deterioration.
Both hot and cold weather applications can result in poor bond between the substrate and repair material.
For more information on how to protect repairs in extreme climates, refer to the following guides:
ACI 305 Guide to Hot Weather Concreting
ACI 306 Guide to Cold Weather Concreting

## Slide 99: Material Properties
Flow Characteristics
Rate of Strength Gain
Exothermic
Working time = how long you have to work with the material after it is mixed and before it begins to set. Also known as “pot life.”
This information is typically provided by the manufacturer and is expressed in minutes.
Constructability
Hot and Cold Weather Applications
Working Time
Other Considerations
Notes: Working time refers to the amount of time after the material is mixed until the material begins to set. Similar to the rate of strength gain, the working time is affected by temperature: the hotter the temperature, the shorter the working time.
This time is determined by the material manufacturer, typically expressed in minutes.

## Slide 100: Material Properties
Flow Characteristics
Rate of Strength Gain
Exothermic
It’s important that the repair materials and surface treatments are compatible with the substrate.
The specifier should identify materials that would pose a compatibility risk and contact the material manufacturer.
A trial application may also pose useful if compatibility is a concern.
Constructability
Hot and Cold Weather Applications
Working Time
Other Considerations
Notes: Verify that the repair materials and surface treatments being used are compatible with the substrate as some repair materials may generate adverse chemical reactions when exposed to substrate conditions.
The specifier should identify those materials which could pose a compatibility risk and determine which repair materials can be used together. The specifier should also question the product manufacturer to determine if the material being evaluated has the potential to react with the substrate being repaired.
This can also be determined by conducting trial applications on a small area.

## Slide 101: Checkpoint Questions
If we go back to our repair scenario, which of the following material properties would be good to have? Select all that apply.
Freezing/thawing resistant
Shrinkage resistant
Abrasion resistant
Compatible with the substrate
Low permeability
Notes: Time provided, ask these Check Your Knowledge Questions. You can hide questions that you do not want to ask prior to the presentation.

## Slide 102: Checkpoint Questions
If we go back to our repair scenario, which of the following material properties would be good to have? Select all that apply.
Freezing/thawing resistant
Shrinkage resistant
Abrasion resistant
Compatible with the substrate
Low permeability
Ideal? Yes!
Feasible?...
Notes: Of course it would be ideal to have a repair material that has all of these properties! However, it is often unrealistic to expect to find a repair substance with all of the desired attributed at a reasonable cost.
In most cases you will need to choose which property is most important for your repair and then choose a repair material that ensures this property is met.

## Slide 103: Optimizing Material Properties
It’s all about balance.
Optimizing one material property is usually at the expense of another, less important material property for the repair at hand.
Notes: It’s best to choose one or two properties you want to enhance while still taking into account your repair material conditions and requirements covered earlier. Maybe you found the perfect product, but its relatively expensive and the owner has expressed many times that he/she wants to keep the cost as low as possible. Maybe this material is more expensive because it is easier to install, thus decrease labor costs and resulting in a cheaper repair. Than this material would be great! However, if the expensive repair material would cost the same to install as a less expensive option and cost is a main factor, you may want to look around for another repair material to use in the job that will be least costly overall.

## Slide 104: Types of Repair Materials
Binder
Holds aggregate together
i.e., cement, epoxy or acrylics
Aggregate:
Gives the material mass
Can be fine or course
Water:
Activates the binder
+
+
Ready-mix concrete is the cheapest and most readily available type of concrete but…
Ready-Mix
“Why not use ready-mix concrete for every repair?”
It is not ideal for most repairs!
Notes: Ready mix concrete is the simplest, most readily available, and inexpensive form of concrete. However, it is often not the best material to use for repairs. When we consider all of the properties a repair material could have, we often want something more than just generic concrete.

## Slide 105: Desired Properties
“So, if I can’t use ready-mix concrete for every repair…how do I find a repair material that has the properties I need?”
When choosing a repair material, you have two options:
Add admixtures to ready-mix concrete
Use proprietary repair materials that are already engineered with admixtures for specific applications.
Because proprietary repair materials are tested and proven solutions, they are more likely to yield a successful repair.
Notes: So you may ask yourself, if I can’t use, just plain concrete for this repair, how do I find a repair material that has the properties I need?
When choosing a repair material, you have two options. You can either add admixtures to ready-mix concrete to enhance its properties, or you can purchase proprietary repair materials that are engineered for specific applications that already have admixtures incorporated.
It is highly recommended to use the second option. Here’s why:
Proprietary repair products have already done all the work for you. They’ve already added admixtures in the right proportions for various applications and eliminated the “guess work” that often occurs when someone is including admixtures on their own. Proprietary products have been tested and evaluated for these specific applications. Therefore, the proprietary repair materials are much more likely to provide a successful repair.

## Slide 106: Admixtures
Accelerating
Retarding
Water-Reducing
Admixtures, or additives, are added to concrete to enhance the effectiveness, constructability, and durability of the repair.
Different admixtures are used depending on which properties you want to enhance.
Refer to the guidelines suggested next to each type of admixture we will cover in the following slides.
Admixtures
Shrinkage Compensating
Corrosion Inhibiting
Air-Entrained Concrete
Lithium Based
Notes: Admixtures, or additives, are added to concrete to enhance the effectiveness, constructability, and durability of the repair.
As we’ve just covered, proprietary repair materials have already incorporated admixtures into the mix, eliminating the guess work.
Different admixtures are used depending on which properties you want to enhance. While it may sound like a good idea to add many of these admixtures to combat different factors, it be best to keep the recipe as simple as possible. We’ll briefly cover different types of admixtures next. For more information refer to the associated references with each admixture covered.
----------------------------------------
Quiz Note
This slide features information that will be found on the post-course knowledge assessment.
True or false: Admixtures are added to concrete to enhance the effectiveness, constructability, and durability of the repair.
True
False

## Slide 107: Admixtures
Accelerating
Retarding
Water-Reducing
Accelerating admixtures increase the rate of hydrating in the repair material.
ASTM C494 (AASHTO M 194)
Admixtures
Shrinkage Compensating
Corrosion Inhibiting
Air-Entrained Concrete
Lithium Based

## Slide 108: Admixtures
Retarding
Water-Reducing
Retarding admixtures decrease the rate of hydration in the repair material.
ASTM C494 (AASHTO M 194)
Admixtures
Shrinkage Compensating
Corrosion Inhibiting
Air-Entrained Concrete
Lithium Based
Accelerating

## Slide 109: Admixtures
Water-Reducing
Water-reducing admixtures reduce the water content needed while maintaining the workability of the repair material.
ASTM C494 (AASHTO M 194)
Admixtures
Shrinkage Compensating
Corrosion Inhibiting
Air-Entrained Concrete
Lithium Based
Accelerating
Retarding

## Slide 110: Admixtures
Shrinkage compensating admixtures reduce the drying shrinkage and related cracking that can occur in the repair material as it cures.
Admixtures
Shrinkage Compensating
Corrosion Inhibiting
Air-Entrained Concrete
Lithium Based
Accelerating
Retarding
Water-Reducing

## Slide 111: Admixtures
Corrosion inhibitors help minimize steel reinforcement corrosion.
Admixtures
Corrosion Inhibiting
Air-Entrained Concrete
Lithium Based
Accelerating
Retarding
Water-Reducing
Shrinkage Compensating
ASTM C1582

## Slide 112: Admixtures
Air-entrained concrete contains microscopic air cells which provide room for water to expand into when the water freezes.
Admixtures
Air-Entrained Concrete
Lithium Based
Accelerating
Retarding
Water-Reducing
Shrinkage Compensating
ASTM C260, ASTM C233
Corrosion Inhibiting

## Slide 113: Admixtures
Admixtures
Lithium Based
Accelerating
Retarding
Water-Reducing
Shrinkage Compensating
Corrosion Inhibiting
Air-Entrained Concrete
Lithium-based admixtures consist of water-soluble salts that are used to help control alkali-silica reactivity (ASR).

## Slide 114: Other Repair Materials
In addition, there are other materials that can be used in the repair process to increase strength and durability.
First, we’ll briefly cover how a surface should be properly prepared.
Notes: Since some of these are applied directly to the prepared substrate after delaminated concrete has been removed, we will briefly cover how a surface should be properly prepared to increase the likelihood of a lasting repair.

## Slide 115: Proper Surface Preparation
INCORRECT
CORRECT
Let’s say this is a diagram of where the concrete has delaminated.
This would be the correct formation to cut.
Simple, rectangular layout
We don’t want to make the concrete “go around corners.” It will crack at these locations.
Notes: The perimeter should be kept as simple as possible, configured in rectangular or square shapes and edges.
Many may resist this and want to cut the perimeter as seen on the right so that they don’t have to remove and replace as much concrete. However, was you can see, highlighted in yellow, cracks will always occur at the weakest point.
If the repair was saw cut in this way, more cracks could have occurred around the repaired area and another repair would need to take place. All of that work would have been for nothing.
Remember, the most simple layout is the best. Concrete cannot go around corners, it will always crack.
You will inevitably have to remove some good concrete to obtain the correct, rectangular formation.

## Slide 116: Proper Surface Preparation
Clearance under corroded rebar should be at least ¾″ (0.75) in.
Undercut
90°
¾
Proper undercutting ensures that the entire rebar is covered in the new repair material.
Be sure to undercut the rebar
Notes: “Concrete removal should continue around the reinforcing steel to create a minimum of 0.75 in. (19 mm) clearance to the surrounding concrete or 0.25 in. (6 mm) larger than the coarsest aggregate in the repair material.”
- p. 9, ACI 546R-14 Guide to Concrete Repair
If reinforcement is corroded, you must cut away the concrete underneath the rebar. The depth of the cut under the rebar should be at least three-fourths of an inch or one-fourth of an inch greater than the largest aggregate size in the repair material, whichever is greater.
----------------------------------------
Quiz Note
This slide features information that will be found on the post-course knowledge assessment.
How much should you undercut the rebar when conducting a structural repair?
1/4" or at least 1/4" greater than the largest aggregate size of the repair mixture, whichever is greater
1/2" or at least 1/4" greater than the largest aggregate size of the repair mixture, whichever is greater
3/4" or at least 1/4" greater than the largest aggregate size of the repair mixture, whichever is greater
1" or at least 1/4" greater than the largest aggregate size of the repair mixture, whichever is greater

## Slide 117: Severe Corrosion of Reinforcing Bar
“If the reinforcing steel has lost more than 25% of its cross section (or 20% if two or more adjacent bars are affected), then reinforcing steel repair is generally required.”
-p. 150, Emmons, Concrete Repair and Maintenance.
If rebar needs repair, either:
Supplemental bar may be added over affected length (known as lap-splicing seen highlighted in red here)
Complete bar replacement
For more information on how to replace severely deteriorated rebar, refer to:
ICRI 310.1 R-2008 Guide for Surface Preparation for the Repair of Deteriorated Concrete Resulting from Reinforcing Steel Corrosion
Notes: According to Peter Emmons book on Concrete Repair and Maintenance, if the rebar has lost more than 25% of its cross section due to corrosion, then the reinforcing steel will need to be repaired.
In this event, the Project Engineer will have one of two options: one can either add a supplemental reinforcing bar along the length of the affected area and attach it to the existing bar. This method is known as lap-splicing. The second option is to completely remove and replace the reinforcing bar. For more information on how to do so, refer to ICRI 310.1 R-2008 Guide for Surface Preparation for the Repair of Deteriorated Concrete Resulting from Reinforcing Steel Corrosion which outlines the best way to deal with reinforcing bar that has deteriorated significantly.

## Slide 118: Proper Surface Preparation
The concrete should be somewhat rough with teeth and open pores that will promote the interlocking of the substances as the repair material cures.
To verify that the surface has been correctly placed, ICRI has created Concrete Surface Profile (CSP) chips that can be used by the installer.
Notes: The concrete should be somewhat rough with teeth and open pores that will promote the interlocking of the substances as the repair material cures.
We also want to be sure that the concrete is cleaned free of laitance and any particles that could interfere with bonding.
The surface should also be saturated-surface dry (SSD), meaning that the surface is damp after cleaning. That being said, there should be no free-standing water that would interfere with the bonding of the repair material.
ICRI has created a concrete surface profile (CSP) chips for determining the surface profile necessary for various repair applications. These chips were originally created to allow the manufacturer of the material to specify the intended substrate.
These chips, seen here, can be compared to the prepared substrate to help contractors and installers verify that the concrete substrate is properly prepared as specified based on the type of substrate being repaired.
The numbers of the chip refer to the size of the aggregate used in the concrete make-up.

## Slide 119: Coating on Reinforcement
primer to protect reinforcing bar
Rebar was undercut, and cleaned of rust and corrosion prior to application of primer.
Undercut
90°
¾
Using a primer
Notes: If deterioration was caused by corrosion of the metal reinforcing bar, it may make sense to provide extra protection over the rebar in order to prevent this from happening again. First, the concrete must be undercut and prepared in the method previous explained.
Primers are coatings on reinforcement that make it more difficult for corrosive agents to reach the rebar.

## Slide 120: Coating on Reinforcement
Zinc-rich rebar primers are sacrificial coatings.
Notes: Zinc-rich primers, for example, are sacrificial coatings. Because zinc is a less noble metal than steel, when the corrosive elements come into contact with the rebar, the zinc coating will corrode instead of the reinforcement, therefore the strength of the structure is not compromised.
Zinc coatings are particularly ideal in areas where corrosive agents are expected (e.g., chemical plants or marine environments).

## Slide 121: What happens if you don’t undercut the rebar?
Coat entire circumference of rebar with primer
Zinc Primer
Steel Rebar
Original Substrate
Repair Material
Area that has corroded away!
No zinc primer
Since zinc primer was not applied under the rebar, not only was the steel not protected, it also experienced accelerated corrosion rates!
No Zinc Primer
INCORRECT APPLICATION OF REBAR PRIMER
Notes: After the reinforcing bar is completely exposed with at least three-fourths of an inch undercut beneath the rebar, the primer should be applied around the entire circumference of the rebar. If you do not completely coat the entire rebar, the corrosive agents will attach a different part of the steel with more intensity.
In this example, the zinc coating did not cover the complete circumference of the steel rebar. The corroding agents attacked the steel with more intensity and eventually, just the zinc coating remained, the steel completely rusted away!

## Slide 122: Bonding Agents
Another type of repair material that is sometimes used in the field is known as a bonding agent.
Some repairs fail because of the inadequate bonding of the repair material at the bond area.
Bonding Agents
Can be applied to prime the substrate to better receive the repair material
Notes: Some repairs fail because of inadequate bonding of the repair material to the substrate. This site is called the bond area.
Bonding agents that can prime the substrate to better receive the repair material.

## Slide 123: The Debate About Bonding Agents
“Why are you using a bonding agent? That’s just one more thing that can go wrong!”
A scrub coat can be just as effective
…it is important to fully coat the edges and apply wet on wet.
If you do decide to use a bonding agent…
Notes: Note that the effectiveness of bonding agents have been disputed in the field. Some say that bonding agents are just “one more thing to go wrong” with the repair and “one more thing to buy.” Research has shown that a good “scrub coat” can often be just as effective as a bonding agent, so if the Project Engineer is looking to decrease the costs of the repair, he or she may consider cutting the bonding agent.
If you do decide to use a bonding agent, it should be applied after surface preparation is complete and before the repair material is placed. It is important that the edges are fully coated. Remember that you should apply the repair material while the bonding agent while it is still tacky. Do not wait for the bonding agent to dry before applying your repair material—if you do so, this could create a bond break instead. We want the bonding agent and the repair material to dry together in order to form a strong bond.

## Slide 124: Surface Treatments
Types of Surface Treatments:
Penetrating Sealers
Surface Sealers
Corrosion Inhibitors
Coatings (High Build and Elastomeric)
Overlays
For more information:
Refer ACI 546R-14 Guide to Concrete Repair
Refer to the Surface Treatments Table on page 10 of your Participant Guide
Notes: Surface treatments can protect and/or enhance the durability of concrete by preventing moisture and chlorides from seeping into the placed repair material.
Surface treatments are particularly recommended in areas that may be subject to deteriorating agents. Chemical plants, marine environments, or concrete subjected to de-icing salts may require extra protection in order to ensure that the damage to the concrete does not reoccur.

## Slide 125: Curing Compounds
For more information refer to:
ASTM C309 Standard Specification for Liquid Membrane-Forming Compounds for Curing Concrete
ACI 308 Guide to Curing Concrete
Curing compounds help concrete maintain adequate moisture while the repair cures.
Notes: Curing compounds are sprayed or rolled directly onto the finished surface immediately following the repair and will eventually dissipate after a set amount of time without staining. This protects the placed repair material from premature drying shrinkage.

## Slide 126: Materials for Crack Repairs
Viscosity
refers to the thickness of a material and is measured in cps.
Peanut butter = 250 cps
Milk = 3 cps
Lower viscosity materials penetrate thin voids easier
Next, we’ll look at materials used for crack repairs…
Notes: Different repair materials are used for cracks that are not associated with delaminated concrete. In addition, certain repair materials should only be used with certain types of cracks. We’ll review the different types of crack repair materials next.
As covered earlier, crack repairs that are not caused by corrosion of the metal rebar and do not require the removal of concrete can use different repair materials. Often, repair materials for cracks typically have a lower viscosity in order to fully penetrate the full depth of the crack. For structural cracks, an injection method may be necessary. Viscosity refers to material thickness and is measured in centipoise (cps). In this example peanut butter has a cps of 250 where as milk has a cps of 3.
It’s important to note that some of crack repair materials should only be used in non-moving cracks, or cracks that will not be subjected to moving forces.

## Slide 127: Types of Cracks
Is the crack moving or non-moving?
Structural
The crack compromises integrity of the structure
Non-Structural
The crack does not compromise the integrity of the structure
Non-moving
Crack will not move
Moving
Repair material allows for some movement of the cracks.
Should be fixed with a flexible material such as a sealant.
Non-moving cracks should be filled with an inflexible material such as an epoxy resin.
Some non-moving cracks can be non-structural
Notes: Whether or not the crack is moving or non-moving will dictate the type of repair material to use.
A non-moving crack, as it’s name suggests will not move. These cracks are typically structural and need to be filled because they compromise the integrity of the structure. Structural, non-moving cracks should be filled with a rigid material under pressure injection to ensure that all voids are completely filled. We will cover this pressure-injection application method later in the course.
Moving cracks, on the other hand, tend to be non-structural, meaning that they do not compromise the integrity of the structure. These cracks still need to be filled, however, as they provide a pathway for deteriorating agents. Moving cracks will constrict and expand for various reasons and should be fixed with a flexible material that will accommodate for some movement. If a moving crack is sealed with an inflexible material, they will possibly crack again adjacent to the repaired crack.

## Slide 128: Crack Repair Materials
Ideal for thin and/or deep cracks
Materials for Structural, Non-Moving Cracks:
Epoxy Resin
ASTM C881 Standard Specification for Epoxy-Resin-Base Bonding Systems for Concrete
Polymer Mortar
ASTM C882 Standard Test Method for Bond Strength of Epoxy-Resin Systems Used with Concrete by Slant Shear
Cement Grout
ASTM C1107 Standard Specification for Packaged, Dry, Hydraulic-Cement Grout (Nonshrink)
Polymer-Cement Mortar
ASTM C1438 Standard Specification for Latex and Powder Polymer Modifiers for use in Hydraulic Cement Concrete and Mortar
Notes: First, let’s look at the types of crack materials that should be used in structural, non-moving cracks. Non-moving, structural cracks that are not associated with delaminated concrete should be filled with a rigid material. For example, a non-moving structural crack could have occurred from an earthquake, or a one-time stress event. The possibility of this event reoccurring and damaging the concrete again in this same way is unlikely.
One of the most common materials used for non-moving structural cracks is an epoxy resin. It is rigid and has a low viscosity and is ideal for pressure injection or gravity feed applications which we will cover later in this course.
Polymer mortars, polymer cement mortars, and cement grouts are all cement-based crack repair materials that are inflexible. These materials are typically used in hand-applied, packed applications for wide cracks or for rout-and-seal applications which we will discuss later in this course. It’s important to remember that these materials will not accommodate for movement as their properties are similar to that of cement.

## Slide 129: Crack Repair Materials
Materials for Non-Structural, Moving Cracks:
Polyurethane Chemical Grouts
ASTM D638 Standard Test Method for Tensile Properties of Plastics
Silicone Sealants
ASTM C920 Standard Test Method for Elastomeric Joint Sealants
Methacrylates
ASTM C882 Standard Test Method for Bond Strength of Epoxy-Resin Systems Used with Concrete by Slant Shear
Polysulfide Sealants
ASTM C920 Standard Test Method for Elastomeric Joint Sealants
Polyurethane (Urethane) Sealants
ASTM C920 Standard Test Method for Elastomeric Joint Sealants
Notes: Materials used in non-structural moving cracks, on the other hand, should be able to accommodate for some movement. For example, let’s say that cars’ heavy loads cause cracks on the surface of a parking garage. These cracks do not damage the structural integrity, nor are they associated with delaminated concrete. Since it is likely that more cars will cause further abrasion and movement on this structure, we do not want to fill these cracks with a non-moving/rigid material that does not accommodate for movement. Indeed, since often the repair material is stronger than the substrate, if a moving crack is filled with a non-moving/rigid material, more cracks will occur around the filled crack.
Polyurethane grouts react with water to form a permanent water-tight seal against deteriorating agents. Sealants are used to fill gaps, keep water at bay, as they allow for 25% to 50% of movement in the crack. Methacrylates are a very low-viscosity (thin) material that are used to fill hairline cracks over a large area. Often this materials is poured over the affected, horizontal area and allowed to pool over the thin cracks, using gravity to help the material penetrate and fill these voids. The excess material is then removed.
----------------------------------------
Quiz Note
This slide features information that will be found on the post-course knowledge assessment.
Which of the following crack repair materials would be suitable for a moving, non-structural crack?
Epoxy resins
Polyurethane chemical grouts
Polymer mortars
Silicone sealants

## Slide 130: Activity
CYK/Questions placeholder
  Can set at below-freezing temperatures
  Will match the substrate in aggregate size
  Has a quick turn-around time
  Will provide a lasting repair
  Will protect reinforcing bar
  Is easy to place
  Has a low cost
What would be some desirable repair materials in our scenario?
We should consider…
Repair mortar with corrosion inhibitors and an accelerating admixture for cold weather applications.
Surface treatments that protect against infiltration of aggressive chemicals.
Reinforcing steel primer to protect against aggressive chlorides.
…that are low cost and relatively easy to place.
?
Notes: Remember that there was delaminated concrete and corrosion of reinforcing bar in our repair scenario, so we would not be looking for a crack repair material to fix this issue.
Ask the audience “What would be some desirable repair materials in our scenario?” After a few answers, show the bulleted list.

## Slide 131: Checkpoint Questions
Concrete with a high water/cement ratio can result in all of the following EXCEPT…
  Increased curing and drying shrinkage
  Reduced abrasion resistance
  Higher risk of shrinkage cracks
  Decreased creep
Notes: Time provided, ask these Check Your Knowledge Questions. You can hide questions that you do not want to ask prior to the presentation.

## Slide 132: Checkpoint Questions
Concrete with a high water/cement ratio can result in all of the following EXCEPT…
  Increased curing and drying shrinkage
  Reduced abrasion resistance
  Higher risk of shrinkage cracks
  Decreased creep
Concrete with a high water/cement ratio can result in increased creep which is undesirable.
Notes: Time provided, ask these Check Your Knowledge Questions. You can hide questions that you do not want to ask prior to the presentation.

## Slide 133: Repair Material Considerations
Be sure to select a repair material that not only fixes the issue, but also has the material properties you desire for the application. This will increase the chances of a lasting repair.
To review:
Notes: Be sure to stop and ask the audience if there are any questions at this time.

## Slide 134: Repair Application Methods

## Slide 135: Concrete Basics
In this lesson we will cover…
  Application methods for replacing delaminated concrete.
  Application methods for fixing cracks in concrete.
  Advantages and disadvantages of these application methods.
  The material properties that should be considered with each application method.
Notes: Review lesson objectives.

## Slide 136: Things to Consider
Let’s say we have a few repair materials that fulfill our requirements.
Material A
Material B
Material C
Now, how do we apply them?
Application Method A
Material
A
Application Method B
Material
A
Material
B
Material
C
Notes: Let’s say that after looking at all the possible repair materials, we select a few candidates of repair materials that have the material properties we desire. Now we have to look at possible application methods. Sometimes the products we select only can be used for a specific placement method. Other times, many materials or application methods can be used interchangeably, depending on the repair.

## Slide 137: Selection
Select repair materials
Select a method of placement
Review the physical properties and placement requirements for the repair material
Change the material or application method as needed.
1
2
3
4
This selection process order comes from ICRI 03731 Guide for the Selecting Application Methods for the Repair of Concrete Surfaces.
Recall the selection process we reviewed earlier. Sometimes it’s not always linear.
Notes: Recall the selection process we reviewed earlier. Sometimes it’s not always linear. The Project Engineer may have to go back and choose another repair material based on the application method he/she selects.

## Slide 138: Methods for Replacement of Delaminated Concrete
The next slides will provide an overview of repair application methods.
Each overview will include:
A general description of the process
Advantages of the method
Disadvantages of the method
For more information for each of these applications, refer to:
ACI 304R Guide for Measuring, Mixing, Transporting, and Placing Concrete
ICRI 03731 Guide for the Selecting Application Methods for the Repair of Concrete Surfaces
Concrete Repair and Maintenance Illustrated by Peter H. Emmons

## Slide 139: Reprofiling Application
Reprofiling Application
Trowel-applied methods seeks to reprofile, or level out a surface.
Best Application: Surface restorations when reinforcing steel is not encountered.
Material Requirements: fine-grained material that can be worked into a ball. It should have non-sag properties so that it can stay in place for the life of the repair.
Notes: The primary purpose of this repair is to correct surface deficiencies and provide the intended design surface. These deficiencies can include nonmoving hairline or plastic shrinkage cracks, small or shallow surface air voids, honeycombs, or rock pockets. More often than not, this is done for aesthetic purposes.
Repair material is mixed into a trowelable, non-sag consistency. Trowels (or other suitable placing tools) are used to transport the repair materials to the prepared substrate. The repair material is pressed into the substrate to develop intimate contact without voids.

## Slide 140: Reprofiling Application
Advantages:
Can be used in vertical and overhead repairs
No formwork necessary
Less equipment is needed than in other repairs
Disadvantages:
Only ideal for areas where reinforced steel is not encountered
Success of repair is dependent on the laborer
For more information, refer to:
ACI RAP-10 Leveling and Reprofiling of Vertical and Overhead Surfaces
Reprofiling Application: Things to Consider
Notes: Remember, this method should not be used in applications in which the reinforcing bar is encountered.

## Slide 141: Hand-Applied (Dry Pack) Application
Hand-Applied (Dry Pack) Application
Trowel-applied methods seeks to reprofile, or level out a surface. This is sometimes known as “dry-packing.”
Best Application: thin or cosmetic repairs for vertical or overhead locations.
Material Requirements: mortars that can be molded into a ball without sagging.
Notes: Hand application repairs are ideal in thin repairs that are cosmetic in nature. Although they can be used in structural repairs, in which repair material must be consolidated around the reinforcing bar (as seen in this image) opinions about the effectiveness of this technique vary. Some recommend that repairs encompassing the reinforcing bar should only use pressurized methods (meaning in a form-and-pour/pump method or shotcrete method, etc.) in order to ensure that the rebar is completely encapsulated without air pockets.
However, because the hand application method is simple, inexpensive, and does not require a variety of equipment, it is favored in many instances. Just remember to consider other methods when repairing around reinforcing bar as hand application will most likely not deliver the best results.

## Slide 142: Hand-Applied (Dry Pack) Application
Advantages:
Can be used in vertical and overhead repairs.
Less expensive than other methods.
Less equipment is needed than in other methods.
Ideal for thin, cosmetic repairs.
Disadvantages:
Can be difficult to consolidate around reinforcing bar.
Success of repair is dependent on laborer.
For more information, refer to:
ACI RAP-6 Vertical and Overhead Spall Repair by Hand Applications
Hand-Applied (Dry Pack) Application: Things to Consider
Notes: Note that this repair is particularly dependent on the skill of the installer. Because if this, with this type of placement method, it may be a good idea to conduct a small, trial installation, to ensure that the installers are familiar with how to properly place the material.

## Slide 143: Spall Repair of Horizontal Surfaces
Spall Repair of Horizontal Surfaces
Repair material is poured into open, properly prepared cavity.
Best Application: horizontal repairs where no framework is required.
Material Requirements: cast-in-place concrete with low shrinkage and a low water-to-cement ratio.
Notes: Unlike shotcrete or form-and-pump applications that are self-consolidating, spall repairs or form-and-pour repairs will need the concrete to be consolidated to ensure that there are no air pockets in the poured material. This can be done using a vibrator as seen here.
In this image, you can see that the installer is pouring towards the middle/right of the repair area. He will need to take care to evenly spread out and consolidate the material over the entire area.

## Slide 144: Spall Repair of Horizontal Surfaces
Advantages:
Common on elevated or on-grade slabs
Low cost (does not require expensive labor or intensive formwork)
Disadvantages:
Laborer needs to ensure proper spacing and consolidation of repair material, particularly at the corners
Curing compounds may be needed
Spall Repair for Horizontal Surfaces: Things to Consider
For more information, refer to:
ACI RAP-7 Spall Repair of Horizontal Concrete Surfaces
Notes: Horizontal surface repair is common on elevated or on-grade slabs. This repair does not require expensive and labor intensive formwork as the parameters of the repair are outlined by the saw-cut perimeter. Although this seems like a simple repair, there are many things that could potentially go wrong. It’s critical to properly prepare the surface prior to placing the repair material. Also, the installer needs to ensure that the repair material is evenly spread out in the cavity, particularly at the corners and is consolidated to ensure that there are no air pockets as these pockets can provide a pathway for disintegrating agents.

## Slide 145: Form-and-Pour Application
Formwork is erected, repair materials are poured into the cavity and consolidated with a vibrator
Best Application: columns, walls, and exterior slabs.
Material Requirements: castable concrete, or mortar, with proper bond properties, low shrinkage, low water-to-cement ratio and is highly flowable.
Form-and-Pour Application
Notes: In form-and-pour applications, formwork is erected and the repair material is poured inside. When selecting a material for this repair, placeability is the primary consideration. Consolidation is also done with vibration of rodding. A trial installation is highly recommended for this type of repair.
Note: It is critical that the formwork is designed and erected so that there is a way for the air to get out as the material is poured. This precaution decreases the chances of air pockets in the finished repair.

## Slide 146: Form-and-Pour Application
Advantages:
Many different materials can be used.
Repair material can be placed around reinforcement.
No potential sagging of materials.
Formwork prevents against early drying which could lead to undesirable cracking.
Disadvantages:
Formwork can be expensive to install and erect, especially in areas that are tricky to get to.
Formwork is more labor intensive.
Poured repair material will still need to be consolidated to ensure that there are no air pockets behind the formwork.
Form-and-Pour Repair: Things to Consider
For more information, refer to:
ACI RAP-4 Surface Repair Using Form-and-Pour Techniques
Notes: Although many different types of repair materials can be used in this repair, the main limitation is that the building of the formwork makes the installation much more labor intensive than other alternative placement methods such as shotcrete or hand application.

## Slide 147: Form-and-Pump Application
Formwork is erected. Repair materials are pumped into the cavity via concrete line until cavity is filled and pressurized.
Best Application: overhead and vertical repairs where congested reinforcement is present.
Material Requirements: pumpable, flowable, self-bonding, with aggregate size compatible with size of cavity and space between bars.
Form-and-Pump Application
Notes: This method of placement is primarily used on vertical surfaces, such as walls or columns. This placement method can also be done as a “full-depth” repair in which an entire piece of concrete needs to be removed and replaced. In this situation, formwork (also sometimes known as shoring) will be erected on both sides of the beam or member and then the repair material is pumped into place. Not that the Project Engineer should take special precautions to ensure that the integrity of the structure is not compromise during the placement and curing process.
----------------------------------------
Quiz Note
This slide features information that will be found on the post-course knowledge assessment.
Which of the following application methods is self-consolidating?
Form and Pour
Form and Pump
Spall Repair of Horizontal Surfaces
Hand Applied

## Slide 148: Form-and-Pump Application
Advantages:
Placement not limited to thickness of repair.
Repair materials are pre-mixed.
No potential sagging of materials.
Formwork prevents against early drying while curing that can result in cracking.
Pressurization consolidates material around rebar.
Disadvantages:
Formwork can be expensive to install and erect, especially in areas that are tricky to get to.
Formwork is more labor intensive.
Form-and-Pump Repair: Things to Consider
Similar disadvantages to the form-and-pour application.
For more information, refer to:
ACI RAP-4 Surface Repair Using Form-and-Pour Techniques
Notes: For this repair, sagging or dropouts of freshly placed materials aren’t an issue because all materials are supported by the formwork during the placement and curing process.
This placement method is ideal for structural repairs because the repair material is consolidated upon placement.
Because the repair material is tightly paced under pressure, this method may be ideal when the reinforcing bar is tightly packed and other placement methods may prove difficult to adequately consolidate around the rebar.
That being said, the formwork can also be expensive and time consuming to erect. The equipment is also costly and may require a more specialized installer.

## Slide 149: Preplaced Aggregate Application
Pre-Placed Aggregate Application
Formwork is erected. Gap-graded aggregate is placed into cavity and then grout is pumped until all voids are filled and pressurized.
Best Application: vertical/overhead applications where extremely low shrinkage of repair material is required. Ideal for underwater applications.
Material Requirements: gap-graded aggregate, pumpable grout, self-bonding cement or binder.
Notes: In the pre-placed aggregate method, coarse aggregate is placed in a form and later grout is pumped in the cavity to fill around the voids of the aggregate under pressure. Most pre-placed aggregate grouts are prepackaged with additives made specifically for this application.

## Slide 150: Preplaced Aggregate Application
Preplaced Aggregate Application: Things to Consider
Advantages:
Can be used for underwater repairs.
Shrinkage can be reduced by 50-100%.
Aggregate is uniformly distributed.
Aggregate can be placed in “hard-to-get” locations.
Disadvantages:
Formwork can be expensive to install and erect especially in areas that are tricky to get to, such as underwater repairs.
Formwork is more labor intensive.
Proper proportioning of the structural grout mixture is necessary.
For more information, refer to:
ACI RAP-9 Preplaced Aggregate Application
Notes: This repair has many advantages, the greatest of which is that it can be placed underwater. Also, because the aggregate is already tightly packed, less cement/grout is used which therefore decreases possible shrinkage. Most preplaced aggregate grouts are prepackaged with additives made specifically for this application.
Erecting formwork is already relatively costly and labor intensive. Since this application can be used for underwater repairs, creating this formwork can be even more costly and more labor intensive than if it were a simple form-and-pump. However, because this application method can decrease potential shrinkage by 50-100% it is often worth the added cost of having skilled laborers.
Refer to the Repair Application Procedure bulletin 9 published by the American Concrete Institute (ACI) for more details on executing this repair.

## Slide 151: Shotcrete Application
Shotcrete Application
There are two types of shotcrete applications: dry-mix and wet-mix shotcrete
Dry-mix: water and admixtures, if any, are introduced at the spray nozzle, just before the repair material is sprayed. It is more ideal for deeper applications and may produce more rebound.
Wet-mix: powder is mixed with water first and then sprayed. This method is more ideal for shallow repairs and offers less rebound.
Notes: Shotcrete applications are among the most economical and effective methods to repair concrete. Although other repair application methods that are self-consolidating require formwork, shotcrete does not. Therefore it is often used when forming requirements are too difficult or too expensive.
There are two types of shotcrete applications.
Dry process and wet process concrete. Each have their advantages.
With dry-process shotcrete, the powder only interacts with the water at the nozzle. This types of shotcrete is ideal for deeper applications because the material is stiffer. It also offers faster set times.
In wet-process shotcrete the powder is mixed with the water before the repair is started. The material is then sprayed into the cavity. This is advantageous because it produces less rebound and less mess, and is better suited for shallow repairs.

## Slide 152: Shotcrete Application
Advantages:
Ideal for hard-to-reach locations.
Ideal for covering large areas.
Fast erection.
Consolidates as it is applied. This is considered the biggest advantage to shotcrete.
Disadvantages:
Can be messy to clean up.
Skilled, certified installer necessary.
Often used when forming requirements are difficult or too expensive
Shotcrete Application: Things to Consider
For more information, refer to:
ACI RAP-12 Concrete Repair by Shotcrete Application
Notes: This technique is typically used on vertical surfaces such as columns, walls, beams, pier caps or overhead horizontal surfaces such as ceilings, beam bottoms, slab soffits, and deck overhangs.
A huge advantage of this method is that the repair material is consolidated as it is applied and does not require formwork for a self-consolidating placement. It’s typically used when forming requirements are difficult or prohibitively expensive from executing.
Proprietary products are available specifically for shotcrete applications.
Refer to the Repair Application Procedure bulletin 12 published by the American Concrete Institute (ACI) for more details on executing this repair.

## Slide 153: Crack Repair
Next, let’s look at placement methods that repair cracks.
Refer to the Crack Repair Materials Table on page 7 of your Participant Guide for more information about materials ideal for certain types of cracks.
Notes: In the previous examples, we looked at repair applications that replaced removed concrete.
In crack applications, however, if no delaminated concrete is found, the crack can be properly cleaned and filled with a suitable repair material.

## Slide 154: Non-Moving and Moving Cracks
Recall from an earlier slide:
Non-moving cracks
Moving cracks
Should be fixed with a flexible material such as a sealant.
Non-moving cracks should be filled with an inflexible material such as an epoxy resin or cementitious material.
First, let’s look at the ways to fix non-moving, structural cracks…
Notes: If the crack is structural, resin should typically be applied under pressure injection.
If moving cracks are fixed with inflexible material, more cracks may appear adjacent to the repaired crack. Generally moving cracks are non-structural.

## Slide 155: Crack Repair by Gravity Feed Resin
General Description: After crack is properly cleaned with compressed air to remove debris, dispense the epoxy until the void is completely filled.
Material Requirements: a non-moving structural material that is highly flowable.
Best Applications: horizontal, structural applications.
Crack Repair by Gravity Feed with Epoxy Resin
For more information, refer to:
ACI RAP-2 Crack Repair by Gravity Feed with Epoxy Resin
ACI 546.3R-14 Guide to Materials Selection for Concrete Repair
ACI 224.1R Causes, Evaluation, and Repair of Cracks in Concrete Structures
ASTM C881 Standard Specification for Epoxy-Resin-Base Bonding systems for Concrete
For non-moving cracks
Notes: Play video.
All cracks must be prepared by cleaning the crack with compressed air to remove debris.
Dispense the epoxy resin into the repair material until it is level with the substrate. Although this is ideal for non-moving cracks, it may not always be suitable for all types of structural cracks. In general, it is best to place materials that seek to fix structural non-moving cracks with pressure injection that uses positive displacement (as we will look at in the next slide). Pressure injection ensures that there are no air pockets in the crack and that the crack is therefore completely sealed from moisture and other disintegrating agents.

## Slide 156: Crack Repair by Epoxy Pressure Injection
For more information, refer to:
ACI RAP-1 Crack Repair by Epoxy Pressure Injection
ACI 546.3R-14 Guide to Materials Selection for Concrete Repair
ACI 224.1R Causes, Evaluation, and Repair of Cracks in Concrete Structures
ASTM C881 Standard Specification for Epoxy-Resin-Base Bonding systems for Concrete
Crack Repair by Epoxy Pressure Injection
General Description: Crack is filled under pressure through ports.
Material Requirements: flowable, pumpable, non-moving material.
Best Applications: vertical/overhead structural cracks.
For non-moving cracks
Notes: Play video.
After applying ports along the crack, inject the epoxy from the lowest port until that port is filled. Move to next port, and continue until entire crack is filled. Break off ports and finish repair.

## Slide 157: Crack Repair Rout and Seal
Rout-and-Seal Applications
General Description: Sometimes known as “crack chasing,” this method uses a saw or router to create a recess over an existing crack. It is then filled with cementitious material or epoxy paste.
Material Requirements: cementitious material or epoxy paste.
Best Applications: non-moving, horizontal crack.
For non-moving cracks
For more information, refer to:
ACI 224.1R Causes, Evaluation, and Repair of Cracks in Concrete Structures
Notes: Rout and seal application are used for non-moving cracks. This application uses a saw or router to create a recess over an existing crack. Since these are non-moving cracks, they can be filled with a cementitious material or epoxy paste.
It is essential to seal these cracks to prevent the intrusion of moisture and chlorides. Sealing these cracks can slow deterioration of the structure and protect the rebar from corrosive agents.

## Slide 158: Crack Repair: Flood Coating
Methyl-Methacrylate Flood Coating
General Description: Hairline cracks filled with a low-viscosity methyl-methacrylate by pouring material over affected area.
Material Requirements: extremely low-viscosity repair material.
Best Applications: horizontal surfaces with shallow, hairline cracks that show no evidence of steel rebar corrosion.
For more information, refer to:
ACI RAP-13 Methacrylate Flood Coat
ACI 224.1R Causes, Evaluation, and Repair of Cracks in Concrete Structures
For non-moving cracks
Notes: Hairline cracks in concrete can occur from a variety of causes. Typically on roads such as this, they can be caused from abrasion (thousands of cars driving over this surface every day), freeze-thaw cycles, or deicing salts. When there are thin cracks, its not always feasible to fill these cracks individually. Therefore, a flood coating it sometimes used. Flood-coating applications pour a very thin repair material (think thin glue) over the surface. The low-viscosity material will then penetrate many hairline cracks at once and seal them from further deteriorating agents.
Methyl-methacrylates are particularly ideal for this type of application.

## Slide 159: Moving Cracks
Now we’ll take a look at how to repair moving cracks…
Possible materials for moving cracks include:
Polyurethane grouts or sealants
Polysulfide sealants
Silicone sealants
Notes: Remember, generally moving cracks are non-structural and need to be filled with a flexible, rubbery material that can accommodate for movement.

## Slide 160: Moving Cracks
When applying repair material to moving cracks there should be no “three-sided adhesion.”
Here the repair material is only attached to two sides of the cracked substrate.
A backer rod can be used
Notes: When applying repair material to moving cracks there should be no “three-sided adhesion.” This is done so that the material can expand and contract horizontally without putting pressure on the bottom of the crack.
Repair material can be applied using a backer rod or bond breaker tape to prevent the repair material from adhering to the bottom of the crack.

## Slide 161: Repair Application Scenario
Let’s go back to our repair scenario. Remembering that we want to keep cost low and that we have novice installers, which repair method would work best?
Preplaced aggregate
Shotcrete
Methyl-methacrylate flood coating
Spall repair of for horizontal surfaces
Form and pump

## Slide 162: Repair Application Scenario
Spall Repair of Horizontal Surfaces
Notes: Spall repair of horizontal surfaces would be a great candidate for this repair because it does not require formwork which can not only be difficult to do for new installers but also very costly. Refer to ACI RAP-7 for more information on the repair application procedure.

## Slide 163: Practice Scenarios
The side of a column in a parking garage has experienced light honey-combing.
The deterioration is contained to the surface and you determine that you will not have to undercut the reinforcing bar.
Based on just this information, which repair method should you select for this application?
  Form and pump
  Trowel applied
  Preplaced aggregate
  Shotcrete
Notes: Time permitting, pose this question to your audience.

## Slide 164: Practice Scenarios
The side of a column in a parking garage has experienced light honey-combing.
The deterioration is contained to the surface and you determine that you will not have to undercut the reinforcing bar.
Based on just this information, which repair method should you select for this application?
  Form and pump
  Trowel applied
  Preplaced aggregate
  Shotcrete
Because the reinforcing bar will not be included in the repair, you can use a trowel to hand-apply the repair material to fill the voids.
Notes: Time permitting, pose this question to your audience.
Answer: B. Because the reinforcing bar will not be included in the repair, you can use a trowel to hand apply the repair material to fill the voids.

## Slide 165: Practice Scenarios
One side of a column in a parking garage has experienced severe deterioration.
The column has patterned cracking and from the cracks there is rust.
Based on just this information, which of the repair method s listed below would you select for the application?
  Dry-packing
  Shotcrete
  Flood coating
Notes: Time permitting, pose this question to your audience.

## Slide 166: Practice Scenarios
One side of a column in a parking garage has experienced severe deterioration.
The column has patterned cracking and from the cracks there is rust.
Based on just this information, which of the repair method s listed below would you select for the application?
  Dry-packing
  Shotcrete
  Flood coating
Based on this information, it sounds as though the embedded metal rebar has corroded. The delaminated concrete will need to be removed and the rebar will need to be cleaned of rust.
Notes: Time permitting, pose this question to your audience.
Answer: B. Based on this information, it sounds as though the embedded metal rebar has corroded. The delaminated concrete will need to be removed and the rebar will need to be cleaned of rust. Because the repair will require that the repair material encase the rebar, we want to make sure we are using a placement method that consolidates the concrete as it places it. A dry- or wet-shotcrete application may be ideal in this case because it can be used in vertical or overhead situations and consolidates the repair material around the rebar as it places it.

## Slide 167: Practice Scenarios
The ceiling in a parking garage has experienced severe deterioration.
When you go to the floor above you see that the deterioration is through the entire depth of the concrete slab.
Based on just this information, which repair method should you select for the application?
  Form and pump
  Trowel applied
  Preplaced aggregate
Notes: Time permitting, pose this question to your audience.

## Slide 168: Practice Scenarios
The ceiling in a parking garage has experienced severe deterioration.
When you go to the floor above you see that the deterioration is through the entire depth of the concrete slab.
Based on just this information, which repair method should you select for the application?
  Form and pump
  Trowel applied
  Preplaced aggregate
Because this job will require a full-depth repair, we will want to set up formwork and shoring that will maintain the integrity of the structure as we replace the material.
Notes: Time permitting, pose this question to your audience.
Answer: A. Because this job will require a full-depth repair, meaning that the entire depth of the slab will need to be removed and replaced, we will want to set up formwork and shoring that will keep the integrity of the structure sound as we replace the material.

## Slide 169: Repair Material Considerations
To review:
When selecting a repair method, consider the advantages and disadvantages of each in order to choose a method that not only fixes the issue, but is also feasible for the constraints of the repair.
Notes: Be sure to stop and ask the audience if there are any questions at this time.

## Slide 170: In Closing

## Slide 171
Assess
1
Plan
2
Prepare
3
Execute
4
There are many variables to take into consideration at each step along the way.
Remember to follow the four-step process introduced at the beginning of the course.
Notes: Review the four-step process introduced at the beginning of this couse.

## Slide 172: Handouts From This Course to Use
This guide includes:
Concrete Condition Checklist
Material Selection Guides:
  Owner Requirements
  Service Conditions
  Application Conditions
Crack Repair Material Table
Surface Treatments Table
If helpful, feel free to refer to Participant Guide in the future.

## Slide 173: References
Technical Guidelines and Reference From:
American Concrete Institute (ACI)
International Concrete Repair Institute (ICRI)
American Society for Testing and Materials (ASTM)
American Association of State Highways and Transportation Officials (AASHTO)
Portland Cement Association (PCA)
IHS Standards Store
Other Resources:
Emmons, Peter H. Concrete Repair and Maintenance Illustrated: Problem Analysis, Repair Strategy, Techniques. Kingston, MA: R.S. Means, 1993. Print.

## Slide 174: Course Completion
Simpson Strong-Tie
This concludes the continuing education course.
For a library of Simpson Strong-Tie courses,
visit strongtie.com/workshops
Notes: Do
Draw the meeting to a close. Hand out literature and business cards.
Say
If you have ongoing projects that you would be interested in reviewing together, please let me know.

## Slide 175: Next Steps!
AIA: For those seeking AIA LU/HSW: You will receive an email with a link allowing access to print your Certificate. Congratulations, you will have earned 2 LU/HSW credits. If your AIA member number has been inserted into your profile, Simpson Strong-Tie will report your credits on your behalf to the AIA. No test is required in order to receive HSW credits.
IACET: For those seeking IACET CEUs: You will receive an email with a link allowing access to print your Certificate of Attendance and instructions directing you to the Simpson Student Center to take the exam before credits can be awarded. Once the exam is taken and passed, you will have earned 0.2 CEUs (2 hours of credit). You can then access your Certificate of Completion from the Course Content tab. You must self-report your credits to your certifying organization or agency.
If you have questions or need assistance, please contact training@strongtie.com.
Notes: Presenter Notes:
Review the email and notification process as outlined in this slide.
AIA LUs:
For those that want AIA HSW credit, be sure to provide your AIA number on the sign-in sheet and Simpson will report your credits to the AIA on your behalf.
No test is required for AIA credit.
CEUs:
For those seeking CEUs, watch for an email with instructions to access the online test. After you have passed the test, you may access your Certification of Completion from the course content tab.
You must self-report your credits to your certifying organization or agency.

## Slide 176: Next Steps!
ICC: For those seeking ICC CEUs: You will receive an email with a link allowing access to print your Certificate. Congratulations, you will have earned 0.2 ICC CEU (2 hours of credit). Please make sure your ICC member number has been inserted into your profile. It is your responsibility to self-report your credits to the ICC. Please retain your Completion Certificate for your records.
IACET: For those seeking IACET CEUs: You will receive an email with a link allowing access to print your Certificate of Attendance and instructions directing you to the Simpson Student Center to take the exam before credits can be awarded. Once the exam is taken and passed, you will have earned 0.2 CEUs (2 hours of credit). You can then access your Certificate of Completion from the Course Content tab. You must self-report your credits to your certifying organization or agency.
If you have questions or need assistance, please contact training@strongtie.com.
Notes: Presenter Notes:
Review the email and notification process as outlined in this slide.
Watch for an email directing you to the Student Center to print your certificate.
No test is required for ICC credit. You must self-report your credits to ICC.
For those seeking general IACET CEUs after you have passed the online test, you may access your Certification of Completion from the course content tab. You must self-report your credits to your certifying organization or agency.