## Slide 1: BUILDER TRAINING SERIES
Mis-Installed Anchors
Notes: Welcome
Welcome to this course on Mis-installed Anchors
Presented by Simpson Strong-Tie

## Slide 2: Credit Information
Professional Development Hours
Simpson Strong-Tie® offers Professional Development Hours for completing this course. No other continuing education or accredited credits are available.
This course offers .5 PDH (1/2 hour of PDH credit)
Notes: Credit Information – Professional Development Hours
Simpson Strong-Tie offers Professional Development Hours for completing this course. No other continuing education or accredited credits are available.

## Slide 3: About this Course
Anchors are used in construction to attach objects and structures to concrete and complete the continuous load path.
This course provides information on:
  the code and anchors
  continuous load path
  different types of anchors
  common mis-installations and remediation
Course Learning Objectives When you have completed this course, you should be able to:
  Identify the purpose and types of anchors
  Define the key elements for proper installation of the different types of anchors
  Recognize the main mis-installations for anchors
Notes: About this Course
Course Description
Anchors are used in construction to attach objects and structures to concrete and complete the continuous load path. This course provides information on what the code states about anchors, reviews the continuous load path, and provides examples for different types of anchors. The course then reviews the most common anchor mis-installations and provides solutions to fix or avoid anchor mis-installations.
Course Learning Objectives
When you have completed this course, you should be able to:
Identify the purpose and types of anchors
Define the key elements for proper installation of the different types of anchors
Recognize the main mis-installations for anchors

## Slide 4: Course Agenda
LESSON 1 Anchorage Overview
LESSON 2 Sill Plate Anchorage
LESSON 3 STHD Anchorage
Notes: Course Agenda
The topics covered in this course include the following:
Lesson 1
Anchor Overview
Lesson 2
Types of Construction Plans
Lesson 3
Parts of the Construction Plan Documents

## Slide 5
Mis-Installed Anchors
LESSON 1
Anchorage Overview
Notes: Lesson 1: Anchorage Overview
This lesson discusses the purpose of anchors, the different types of anchors, and the importance of installing them correctly.

## Slide 6: R301.1 Application
Buildings and structures, and parts thereof, shall be constructed to safely support all loads, including dead loads, live loads, roof loads, flood loads, snow loads, wind loads, and seismic loads as prescribed by this code. The construction of buildings and structures in accordance with the provisions of this code shall result in a system that provides a complete load path that meets the requirements for the transfer of loads from their point of origin through the load-resisting elements to the foundation. Buildings and structures constructed as prescribed by this code are deemed to comply with the requirements of this section.
Notes: R301.1 Application
Section R301.1 from the 2018 IRC code states ““The construction of buildings and structures in accordance with the provisions of this code shall result in a system that provides a complete load path that meets the requirements for the transfer of loads from their point of origin through the load-resisting elements to the foundation.” Similar wording is also found in the IBC code.

## Slide 7: The Continuous Load Path
In order to create a complete or continuous load path referenced in the code, the roof must be secured to the upper story, the upper story to the first floor, and the structure to the foundation.
The load path is not complete until the loads are properly transferred to the foundation, which is why anchors are essential.
Secure Roof to
Upper Story
Secure Upper Story
to First Floor
Secure Structure
to Foundation
Notes: The Continuous Load Path
In order to create a complete or continuous load path referenced in the code, it is necessary to secure the roof to the upper story, secure the upper story to the first floor, and secure the structure to the foundation. The load path is not complete until the loads are properly transferred to the foundation, which is why anchors are essential.
(Student Handbook Material)

## Slide 8: The Importance of Anchors
Anchors are important for any structure designed to meet the I Codes and complete the load path into the foundation.
Notes: The Importance of Anchors
Anchors are an important and crucial part of any structure that is designed to meet the I Codes and complete the load path into the foundation.
The next few slides review a variety of anchor system installations available for residential construction buildings.

## Slide 9: Anchor Examples: Holdowns
Anchors are embedded into the concrete and connected to holdowns.
The Strap-Tie Holdown is partially embedded into the concrete. The remaining section is connected to the wood framing.
Strap-Tie Holdown
Anchors Connected to Holdowns
Notes: Anchor Examples: Holdowns
The anchors on this slide are connected to hold downs and then embedded into the concrete to complete the load path.
The Strap-Tie Holdown is partially embedded into the concrete and the remaining section is connected to the wood framing to complete the load path.
(Student Handbook Material)

## Slide 10: Anchor Examples: Column Caps
CCQM and ECCQ column caps for grout-filled CMU and concrete piers.
These connectors incorporate anchors to transfer the required load to the foundation.
ECCQ Column Cap
CCQM Column Cap
Notes: Anchor Examples: Column Caps
These two examples demonstrate the Simpson Strong-Tie CCQM and ECCQM column caps for grout-filled CMU and concrete piers. These connectors also incorporate anchors to transfer the required load to the foundation.
(Student Handbook Material)

## Slide 11: Anchor Examples: Sill Plate Anchors
Sill plate anchored into the foundation
Anchors used in pre-fabricated shear walls
Anchors required to secure a post base connection.
Post Base Anchor
Pre-fabricated Shear Wall Anchor
Sill Plate Anchor
Notes: Anchor Examples: Sill Plate Anchors
The three examples on this slide illustrate the sill plate anchored into the foundation, the anchors used in pre-fabricated shear walls, and the anchors required to secure a post base connection. All of these examples complete the load path to the foundation.
(Student Handbook Material)

## Slide 12: Purpose of Anchors
Anchors transfer the load from the structure to the foundation.
Load transfer into the foundation may include dead, live, wind, flood, snow, and seismic loads.
Anchors transfer loads in two directions:
Tension - when the load is applied parallel to the anchor (shown on the Z axis)
Shear - when the load is applied perpendicular to the anchor (shown on the X and Y axis)
Notes: Purpose of Anchors
The purpose of anchors is to transfer the load from the structure to the foundation. Load transfer into the foundation in a residential building may include dead, live, wind, flood, snow, and seismic loads.
Anchors transfer loads in two directions:
Tension - when the load is applied parallel to the anchor as shown on the Z axis in the figures
Shear - when the load is applied perpendicular to the anchor as shown on the X and Y axis in the figures

## Slide 13: Purpose of Anchors
ONE ANCHOR
One Anchor - may transfer shear or tension.
Group of Anchors with a Base Plate - can transfer shear, tension, or moment. The actual anchor forces are still either tension or shear.
GROUP OF ANCHORS WITH A BASE PLATE
Notes: Purpose of Anchors
One Anchor: A single anchor may transfer shear or tension.
Group of Anchors with a Base Plate: Anchors can transfer shear, tension, or moment when a group of anchors work together with a base plate. The actual anchor forces are still either tension or shear.

## Slide 14: Two types of Anchors
Cast-in-Place - set in wet concrete.
Post-installed - installed into drilled holes after the concrete has cured.
Notes: Types of Anchors
There are two main types of anchors:
Cast-in-place anchors are set in wet concrete.
Post-installed anchors are installed into drilled holes after the concrete has cured for a certain amount of time.

## Slide 15: Cast-in-Place Anchors
Excellent performance and low cost; can be challenging to position, difficult to inspect.
Simpson Strong-Tie’s anchors (below) have been tested for a specific load capacity in tension and shear.
STHD Strap-Tie Holdown
MASA/MASAP
Mudsill Anchors
LMAZ/MAB/MASB
Mudsill Anchors
Notes: Cast-in-Place Anchors
Cast-in-place anchors offer excellent performance and low cost. However, they can be challenging to position and are difficult to inspect.
Simpson Strong-Tie offers several proprietary cast-in-place anchors, such as the mudsill and strap-tie holdown anchors shown here. These anchors have been tested to an acceptance criteria for a specific load capacity in tension and shear.
(Student Handbook Material)

## Slide 16: Cast-in-Place Anchors
J-bolts and L-bolts can be designed by industry standards
Capacity in both tension and shear can be calculated.
Various Cast-in-Place Anchors
Notes: Cast-in-Place Anchors
There are also standard cast-in-place anchors, such as J-bolts and L-bolts, which can be designed by industry standards and the capacity in both tension and shear can be calculated.

## Slide 17: Post-installed Anchors
Offer precise placement and high strength.
Inspection friendly, available in a variety of types, and “Meet the Intent of the Code”.
Load capacity options:
  Masonry construction
  Concrete construction
Notes: Post-installed Anchors
Post installed anchors offer precise placement and high strength. They are inspection friendly, available in a variety of types, and “Meet the Intent of the Code”.
Simpson Strong-Tie offers many post-installed proprietary anchors. There are two options for load capacity: those anchors that have been tested to an acceptance criteria for a specific load capacity in tension and shear for masonry construction, or those with a set of parameters and values that can be used by designers to calculate their capacity based on industry standards when anchored into concrete.

## Slide 18: Post-installed Anchors
Mechanical Expansion anchors (Strong-Bolt® 2)
Mechanical screw anchors (Titen family)
Adhesive Anchors (SET-3G™, AT-XP®, SET-XP® and ET-HP®).
STB2 Mechanical Expansion Anchor
Titen HD® / Titen HD® Rod Hanger Titen Turbo™ Mechanical
Screw-In Anchor
SET-3G™ / AT-XP®
SET-XP® / ET-HP®
Adhesive Anchors
Notes: Post-installed Anchors
The most common types of post installed Simpson Strong-Tie anchors are:
Mechanical Expansion anchors, such as the Strong-Bolt® 2
Mechanical screw anchors, which include the Titen family, and
Adhesive anchors, which include SET-3G™, AT-XP®, SET-XP® and ET-HP® anchors
(Student Handbook Material)

## Slide 19: The Importance of Correctly Installed Anchors
Notes: The Importance of Correctly Installed Anchors
Since anchors are an integral part of buildings and structures, proper installation is extremely important. Always follow the manufacturer’s installation instructions so that the installed anchors meet the listed load capacity or meet the intent of the code when used in a prescriptive code.

## Slide 20: Following Installation Structural Details
Follow installation parameters to meet the intended loads.
These parameters include:
  Edge distance
  Embedment length
  Torque
  Concrete cover
  Hole preparation
  Hole diameter
Notes: Following Installation Structural Details
When the anchors are cast-in-place or post installed, they have been designed and tested within certain parameters. These parameters must be followed during installation for anchors to meet the intended loads.
These parameters include:
Edge distance
Embedment length
Torque
Concrete cover
Hole preparation
Hole diameter

## Slide 21: Check Your Knowledge
What is a post-installed anchor?
An anchor that is set into wet concrete before it sets.
An anchor that is set partially into wet concrete and then attached to the wood framing.
An anchor that is installed into drilled holes after the concrete cures for some time.
Notes: Check Your Knowledge

## Slide 22
Mis-Installed Anchors
LESSON 2
Sill Plate Anchorage
Notes: Lesson 2: Sill Plate Anchorage
This lesson discusses the requirements, specifications, and common mis-installation of Sill Plate anchorage applications.

## Slide 23: Sill Plate Anchorage Requirements
R403.1.6 – Foundation Anchorage
Wood sole plates at all exterior walls on monolithic slabs, wood sole plates of wall brace wall panels at building interiors on monolithic slabs, and all wood sill plates:
Minimum ½” diameter anchor bolt
Minimum 6’ on center spacing
Approved anchors or anchor straps equivalent to ½” diameter anchor bolts
Minimum 7” embedment into concrete
Located in the middle 1/3 of the width of the plate
A nut and washer at each anchor bolt
2 bolts minimum per plate section
12” max or less than 7 times diameter from end of each plate
Interior wood sole plate not part of the braced wall panel positively anchored with approved fasteners
Non-seismic Installations
Notes: Sill Plate Anchorage Requirements – Non-seismic Installations
The IRC Section R403.1.6 contains requirements for anchorage in non-seismic areas. The requirements cover anything less than seismic design Category D for residences and less than seismic design Category C for townhomes.
Wood sole plates at all exterior walls on monolithic slabs, wood sole plates of wall brace wall panels at building interiors on monolithic slabs, and all wood sill plates must be anchored to the foundation with a minimum ½” diameter anchor bolt, spaced not greater than 6 feet on center, or approved anchors or anchor straps are required to provide equivalent anchorage to ½” diameter anchor bolts.
Bolts must extend not less than 7” into concrete or grouted cells of concrete masonry units. The bolts must be located in the middle third of the width of the plate. A nut and washer must be tightened to each anchor bolt. There must be at least 2 bolts per plate section, with one bolt located not more than 12 inches or less than 7 times the diameter from the end of each plate. Interior bearing walls that are not part of the braced wall panel on a monolithic slab must be positively anchored with approved fasteners.

## Slide 24: Sill Plate Anchorage Requirements
Seismic Installations
R403.1.6.1 – Foundation Anchorage
All walls part of a braced wall line (exterior and interior)
½” diameter anchor bolt
Minimum 7” embedment
Minimum 6’ spacing
Located in middle 3rd
A nut and plate washer 0.229” x 3” x 3”
2 bolts minimum per plate section
12” max from end
7 x diameter min distance from end
Approved anchor
Approved anchor strap
Interior load bearing walls
Same requirement as non-seismic braced wall panel
Residence over two stories in height
minimum anchor bolt spacing of 4’
Notes: Sill Plate Anchorage Requirements – Seismic Installations
The IRC Section R403.1.6.1 has requirements for anchorage for seismic areas which cover wood and light frame structures in seismic design Category D0, D1 and D2 and wood light frame townhouses in seismic design Category C.
The main difference is that all walls within a braced wall line must have an additional 3x3 plate washer at each anchor and all interior bearing walls need to be anchored with bolts, regardless if they are part of a braced wall panel. Also, for any residence over two-stories, spacing of the anchors is 4’ minimum.

## Slide 25: Anchor Spacing
Before the concrete is poured, trying to locate the ½” L-bolt anchor per the code is difficult. The Concrete contractor doesn’t know where the splices of the sill will occur or what length of lumber will be used to locate the anchors within the code spacing.
Anchors have minimum edge distances, end distances, and spacing requirements to consider.
Common mis-installations include missing anchors, oversized holes in the sill plate, and anchors that are not within the proper edge distances.
IRC Code Requirements
Notes: Anchor Spacing – Code Requirements
This illustration shows the required spacing and locations of anchors according to the IRC.
The main difficulty is that during construction, before the concrete is poured, trying to locate the ½” L-bolt anchor per the code is difficult. The Concrete contractor does not know where the splices of the sill will occur or what length of lumber will be used, to accurately locate the anchors within the code spacing.
Another difficulty is that the anchors have minimum edge distances, end distances, and spacing requirements to consider.
For this application, common mis-installations include missing anchors, oversized holes in the sill plate, and anchors that are not within the proper edge distances. The next set of slides reviews these conditions in more detail.

## Slide 26: Cast-in-Place Mis-installation
Not in the middle third of the sill plate that will be installed.
Notes: Cast-in-Place Mis-installation – Middle Third of Sill Plate
In this picture, the cast-in-place anchors were not installed inline, and it does not appear that the anchor on the left side will remain within the middle third of the installed sill plate.
(Student Handbook Material)

## Slide 27: Cast-in-Place Mis-installation
Bolt was too short to attach the washer and nut.
Bolt too short
Distance between the end of the sill plate and the centerline of the bolt is shorter than 3 ½” (required 7x bolt diameter).
Notes: Cast-in-Place Mis-installation – Bolt Too Short
In this picture, the cast in place anchor did not extend above the concrete far enough to be able to properly install the washer and nut. Also, it appears that the distance between the end of the sill plate and the centerline of the bolt is shorter than 3 ½”, which would be 7 times the bolt diameter.
This mis-installation places the integrity of the sill plate in jeopardy and has a high probability of not completing the load path.
(Student Handbook Material)

## Slide 28
Cast-in-Place Mis-installation
Notching reduces the integrity of the studs.
Notched studs to accommodate the anchor bolts
Notched studs to accommodate the anchor bolts.
Notes: Cast-in-Place Mis-installation – Notched Studs
In this picture, the cast in place anchor is at the same location as the studs. In addition, the studs have been notched to accommodate the bolts, greatly weakening the integrity of the studs. This installation has a high probability of not completing the load path.

## Slide 29: Cast-in-Place Mis-installation
Remediation:
The contractor can treat it as an end of sill plate piece and install a post-installed anchor on each side of the notch.
Notched Sill Plate
Sill plate notched to accommodate the anchor.
Notes: Cast-in-Place Mis-installation – Notched Sill Plate
In this picture, the anchor missed the middle third of the sill plate location, and the sill plate was notched to accommodate the bolt. This mis-installation jeopardizes the integrity of the sill plate and does not complete the load path.
To fix this installation, the contractor can treat it as an end of sill plate piece and install a post-installed anchor on each side of the notch.

## Slide 30: Post-Installed Anchor Mis-installation
Using an expansion anchor to anchor exterior wall sill plates is not recommended.
Expansion anchors work by expanding the bottom clip, which creates tensile forces in the concrete below.
Installation in the middle of the slab is fine.
Installation close to the edge of the slab may result in spalling.
Too Close to Edge
Spalling of the concrete due to expansion anchor and bolt placement.
Notes: Post-installed Anchor Mis-installation – Too Close to Edge
In this picture, the expansion wedge anchor is installed too close to the edge of the concrete. Using an expansion anchor to anchor exterior wall sill plates is not recommended.
Expansion anchors work by expanding the bottom clip, which creates tensile forces in the concrete below. When installed in the middle of the slab, there is no problem. However, when installed close to the edge of the slab, it can spall the concrete as shown here.
The minimum edge distance for a ½” Strong-Bolt 2 anchor is 4”, so this installation design would not be able to achieve the full capacity load of the anchor. The ½” Wedge-All anchor has a minimum edge distance of 2”. However, there is a reduction of 70% in shear capacity and 30% reduction in tension when installed this close to the edge. Note that sill plate anchors are typically used for shear resistance and are not ideal for this application.
(Student Handbook Material)

## Slide 31: Post-Installed Anchor Mis-installation
Strong-Bolt 2 anchor is installed too close to the concrete edge.
Minimum edge distance for a ½” Strong-Bolt 2 anchor is 4”.
The ½” Wedge-All anchor has a minimum edge distance of 2”. However, there is a reduction of 70% in shear capacity and 30% reduction in tension when installed this close to the edge.
Sill plate anchors are typically used for shear resistance and are not ideal for this application.
Too Close to Concrete Edge
Spalling of the concrete due to expansion anchor and bolt placement.
Notes: Post-installed Anchor Mis-installation – Too Close to Concrete Edge
In this picture, the expansion wedge anchor is installed too close to the edge of the concrete. Using an expansion anchor to anchor exterior wall sill plates is not recommended.
Expansion anchors work by expanding the bottom clip, which creates tensile forces in the concrete below. When installed in the middle of the slab, there is no problem. However, when installed close to the edge of the slab, it can spall the concrete as shown here.
The minimum edge distance for a ½” Strong-Bolt 2 anchor is 4”, so this installation design would not be able to achieve the full capacity load of the anchor. The ½” Wedge-All anchor has a minimum edge distance of 2”. However, there is a reduction of 70% in shear capacity and 30% reduction in tension when installed this close to the edge. Note that sill plate anchors are typically used for shear resistance and are not ideal for this application.

## Slide 32: Solutions to Prevent Mis-installation
Recommended solution: use a MASA or LMAZ anchor. Both are easy to install before pouring the concrete and have been evaluated to be a 1:1 replacement to the prescriptive ½” diameter anchor from the code.
The anchorage does not need to be in the middle third of the sill plate.
The only disadvantage of a cast-in place solution is not knowing where the sill plate splice will happen.
Notes: Solutions to Prevent Mis-installation
The recommended solution for sill plate anchorage and prevention of mis-installations for a Cast-In-Place solution, is to use either a MASA or LMAZ anchor. Both are easy to install before pouring the concrete and have been evaluated to be a 1:1 replacement to the prescriptive ½” diameter anchor from the code. Another advantage is that the anchorage is not dependent on having to be in the middle third of the sill plate.
The only disadvantage of a cast-in place solution is knowing where the sill plate splice will happen.

## Slide 33: Post-Install Solution
Simpson Strong-Tie recommends a post install solution as the best option available.
Titen HD® (mechanical screw-in anchor), provides a 1:1 replacement to the prescriptive ½” diameter anchor from the code. The Titen HD is easy to install and can be installed 1¾” from the edge.
SET 3-G™ (adhesive anchor) has the same benefits as Titen HD.
Titen HD (H) hex-washer head
Titen HD (WH) flat-washer head
Notes: Post-Install Solution
Simpson Strong-Tie recommends a post install solution as the best option available. A mechanical screw-in anchor such as the Titen HD, provides a 1:1 replacement to the prescriptive ½” diameter anchor from the code. The Titen HD is easy to install and can be installed 1 ¾” from the edge.
A secondary option is to use an adhesive anchor such as the SET 3-G, which also has the same benefits as the Titen HD for this application.

## Slide 34: SST Technical Bulletin
For Sill Plate anchorage solutions that meet the intent of the code. The PDF document is available on the Resources Tab.
Code Compliant Sill Plate Anchorage Solutions for Concrete and Masonry
Technical Bulletin
T-A-SILPLANCH21
Notes: Simpson Strong-Tie Technical Bulletin
For more information, view the Simpson Strong-Tie Technical Bulletin for Sill Plate anchorage solutions that meet the intent of the code. The PDF document is available on the Resources Tab.

## Slide 35: Check Your Knowledge
Which of the following is a good option to prevent mis-installation of sill plate cast-in-place anchors?
Use a Titen HD cast-in-place anchor.
Use a MASA or LMAZ cast-in-place anchor.
Use a Set 3-G cast-in-place anchor.
Notes: Check Your Knowledge

## Slide 36
Mis-Installed Anchors
LESSON 3
STHD Anchorage
Notes: Lesson 3: STHD Anchorage
This lesson discusses the requirements, specifications, and common mis-installation of Strap-Tie Holdown anchorage applications.

## Slide 37: STHD Strap-Tie Holdowns
Used for Braced Wall Panels – Portal Frame with Holdowns, or PFH.
PFH requires two 3500 lb. strap-type holdowns embedded into the concrete, nailed into the framing (detailed in section R602 of the IRC).
Notes: STHD Strap-Tie Holdowns
The most common application for the STHD is building the prescribed Braced Wall Panel method – Portal Frame with Holdowns, or PFH. PFH requires two 3500 lb. strap-type holdowns embedded into the concrete and nailed into the framing and is detailed in section R602 of the IRC.

## Slide 38: Strap-Tie Holdown Mis-Installation
STHD strap may be bent only one full cycle – bent horizontal once and then vertical for placement.
Note the spalling of the concrete below the bend. If the spall is 1" or less, measured from the embedment line to the bottom of the spall, full loads apply.
STHD10 and STHD14 achieve full load for spalls less than 4".
Improper Bends
Straps bent improperly during installation.
Strap bent improperly during installation.
Notes: STHD Mis-installation – Improper Bends
In this picture, the STHD strap was bent during installation. The proper installation allows the strap to be bent only one full cycle – bent horizontal once and then vertical for placement. In this picture it has been bent more than once.
There is also spalling of the concrete below the bend. If the spall is 1" or less, measured from the embedment line to the bottom of the spall, full loads apply. STHD10 and STHD14 achieve full load for spalls less than 4".
(Student Handbook Material)

## Slide 39: Strap-Tie Holdown Mis-Installation
Note the concrete spalling below the bend.
The spall appears to be about 4”.
If this is an STHD10 or STHD14 this installation would not achieve full load capacity.
Spalling
Spalling of concrete below the STHD.
Spalling of concrete below the STHD.
Notes: STHD Mis-installation - Spalling
In these pictures, the STHD has spalling of the concrete below the bend. The spall appears to be about 4”. If the STHD is a STHD10 or STHD14 this installation would not achieve the full load capacities.
(Student Handbook Material)

## Slide 40: Strap-Tie Holdown Mis-Installation
STHD was installed at an angle before the pour and therefore the straps are not straight.
Based on the amount the straps are leaning, they may not be able to fasten into the studs behind the wall, only the sheathing.
Straps not Straight
Straps were not installed straight to fasten properly to the studs.
Notes: STHD Mis-installation – Straps not Straight
In this picture, the STHD was installed at an angle before the pour and therefore the straps are not straight. Based on the amount the straps are leaning, they may not be able to fasten into the studs behind the wall, only the sheathing.
(Student Handbook Material)

## Slide 41: Strap-Tie Holdown Mis-Installation
The strap is not at the edge of the wall segment. The strap will only be fastened to the sheathing.
The drawing shows the strap being correctly fastened to the studs behind the wall.
Strap Doesn’t Reach Framing
Strap does not reach the framing member.
Notes: STHD Mis-installation – Strap Doesn’t Reach Framing
In this picture, the strap is not at the edge of the wall segment. Note how the PFH detail shows the strap being fastened to the studs behind the wall. However, in this case the strap will only be fastened to the sheathing.
(Student Handbook Material)

## Slide 42: STHD StrapMate
The orange StrapMate ensures that the STHD stays in place during the concrete pour and also reduces spalling of the concrete.
Spall Reduction System
Notes: Slide 45 – STHD StrapMate – Spall Reduction System
Most of the STHD mis-installations are due to either misplacement of the strap-tie holdown before the concrete pour or the spalling of the concrete.
The best way to avoid both of these mis-installations is to use the Simpson Strong-Tie StrapMate shown here. This product ensures that the STHD stays in place during the concrete pour and also reduces spalling of the concrete.

## Slide 43: Holdown PFH
The Portal Frame with Holdown PFH may be used. Simpson Strong-Tie’s solution is the Site Built Portal Frame System, or PFS. This provides an easy way to meet code-required wall-bracing with narrow wall widths. The solution has been evaluated to replace the PFH method while still meeting the intent of the code.
Alternative to STHD
Notes: Holdown PFH – Alternative to STHD
Another alternative is the Portal Frame with Holdown PFH, with the Simpson Strong-Tie Site Built Portal Frame System, or PFS. This option provides an easy way to meet code-required wall-bracing with narrow wall widths. The solution has been evaluated to replace the PFH method while still meeting the intent of the code.

## Slide 44: Check Your Knowledge
When building the prescribed Braced Wall Panel using the STHD the code requires __________.
2500 lb. strap-type holdowns embedded into the concrete every 6”
two 3500 lb. strap-type holdowns embedded into the concrete and nailed into the framing
Four 2000 lb. strap-type holdowns attached as bracing for the framing
Notes: Check Your Knowledge

## Slide 45: Summary
This training covers anchors and mis-installations.
Lesson 1 Overview of anchors and Continuous Load Path Purpose and different types of anchors
Lesson 2 Sill Plate anchors Common mis-installations and remediation.
Lesson 3 Strap-Tie Holdown anchors Common mis-installations and remediation.
Notes: Summary
This training covered many different topics for the product line.
Lesson One provided an overview of anchors and reviewed the Continuous Load Path outlined in the codes. The lesson discussed the purpose of anchors and the different types of anchors available for residential building construction.
Lesson Two provided information on Sill Plate anchors and presented the most common types of mis-installed anchors for this application and discussed how to avoid mis-installations.
Lesson Three provided information on Strap-Tie Holdown anchors and presented the most common types of mis-installed anchors for this application and how to avoid mis-installations.

## Slide 46: Congratulations!
You have completed this course.
S170-SST-02_MIA_v01 Copyright © 2023 Simpson Strong-Tie. All rights reserved.
Notes: Congratulations!
Congratulations! You have completed this course. Use the Exit button to close the training.