## Slide 1
Concrete Properties & Deterioration
Notes: Before we jump into concrete repair, we’re going to spend 15 minutes to talk about the causes of the issue.

## Slide 2: Objectives
Explain the factors that influence concrete behavior
Identify causes of deterioration, damage and defects in concrete
Notes: Here are the topics we’re going to run through briefly…

## Slide 3: Why Does Concrete Deteriorate?
Causes of deterioration are complex
Proper maintenance can prolong life, but doesn’t always get done!
Concrete is under attack from variety of sources
Notes: The deterioration of concrete is more complex than the deterioration of other building materials, such as wood or steel. Normal life expectancy of concrete is 50 years, and many structures today are beyond their life expectancy. Although proper maintenance can prolong concrete life, this often doesn’t get done for one reason or another. Concrete structures are under attack from a variety of sources that we will cover in the following slides.

## Slide 4: Factors that Influence Concrete Behavior
Effects are the result of a combination of these factors
Exposure Conditions
Service Conditions
Service Loads
Design, Materials, & Construction
Notes: It is typically a combination of the following factors that influence concrete:
Exposure Conditions
Service Conditions
Service Loads
Design Materials & Construction - Defects in concrete often happen as a result of issues with design, materials, and construction methods. Things like improper rebar placement, cold joints, or the addition of too much water in the concrete mix can all lead to defects.

## Slide 5: What are the Effects?
  Cracks
  Spalls
  Leakage
  Wear
  Scaling
  Settlement
  Deflection
  Disintegration
Notes: Review some of the effects or behaviors of concrete deterioration listed on this slide.
The root cause of these behaviors can be categorized as Deterioration, Damage, or Defects.

## Slide 6: Common Causes
Freeze-thaw cycles
Erosion
Alkali-aggregate reaction
Sulfate attack
Overloading
Chemicals
Earthquake and fire
Embedded metal corrosion…
Notes: All of the following are deteriorating agents:
Freeze-thaw cycles
Erosion
Alkali-aggregate reaction
Sulfate attack
Corrosion of embedded metals
Overloading, chemical attack, earthquakes and fires are all possible source of damage as well.
Steel rebar corrosion is a big issue, let’s look at that in a little more detail.

## Slide 7: Embedded Metal Corrosion
Chlorides penetrates with help of moisture
Corroding reinforcing steel rebar
Cracks provide access for surface-introduced chlorides
Cracking and spalling of the concrete
Corrosion  Expansion  Cracking of Concrete
Notes: Chloride begins penetrating through the surface with the help of moisture.
As corrosion builds, it pushes the surrounding concrete out and causes cracks.
When cracking and delamination progress, accelerated corrosion takes place because of the easy access of corrosive salts, oxygen, and moisture.
The image shows the build-up of corrosion on the rebar and the cracking effect it has on the surrounding concrete.

## Slide 8: Corrosion-Induced Cracking and Spalling
Depends on the following variables:
    Concrete tensile strength
    Bond between rebar and surrounding concrete
    Diameter of rebar
    Percentage of corrosion by weight of rebar
    Quality of concrete covering rebar…
Notes: If the embedded steel rebar corrodes, it can cause cracking and spalling of the concrete.
This often depends on the following variables:
  Concrete tensile strength
  Bond between rebar and surrounding concrete
  Diameter of rebar
  Percentage of corrosion by weight of rebar
  Quality of concrete covering the rebar…what affects the quality of the concrete? One major factor is the amount of water used in the concrete mix…

## Slide 9: Water to Cement Ratio
More water = lower quality concrete
Excessive water:
reduces strength
increases curing and drying shrinkage
increases porosity
increases creep
reduces the abrasion resistance of concrete
Notes: The use of excessive water in concrete mixtures is one of the most common root causes of damage. Damage caused by excessive mix water can be difficult to correctly diagnose because it is usually masked by damage from other causes.
Excessive water:
reduces strength
increases curing and drying shrinkage
increases porosity
increases creep
reduces the abrasion resistance of concrete
Excessive water is often overlooked as the root cause of the problem. Freeze-thaw cracking, erosion deterioration, or drying shrinkage cracking, for example, is often blamed for damage to concrete when, in reality, excessive mix water caused the low durability that allowed these other causes to attack the concrete.

## Slide 10: So how does it get fixed?
Bosch tools to prepare for a repair
Simpson Strong-Tie products to complete the repair
Notes: (Hand-off to Bosch rep to discuss surface prep and Bosch line up of grinders, accessories ad dedicated tools for concrete repair. We’ll then follow with more about the repair process and RPS product line.)