## Slide 1
Repair, Protection and Strengthening Systems for Concrete and Masonry
Notes: Before we get started, note that you may hear “RPS”, and to us that means Repair, Protect, Strengthen.

## Slide 2: Agenda
Concrete repair process
RPS product overview
Product Guide overview
Notes: Here are the topics we’re going to run through in our short time.
(Learning Objectives) You should walk away from this being able to:
Provide an overview of the concrete repair process
Describe the types of RPS solutions offered by Simpson
Navigate RPS literature to find more information

## Slide 3: Concrete Restoration Opportunities
What are we looking for?
Cracks
Spalled Concrete
Delamination
Rust bleed on the concrete
Efflorescence
Chalky Coatings
Freeze Thaw Damage
Fire Damage
Wind & Seismic Damage
Chemical Attack
Notes: There are some newer things to be on the look out for on the jobsite – no longer just anchoring. There may be an opportunity for concrete repair products.

## Slide 4: Concrete Repair Process
ASSESS
PLAN
PREPARE
EXECUTE
Determine the Problem
Evaluate the Cause
Engineer the appropriate Solution
Complete the Preparation
Complete long term Repair
Notes: Although every concrete repair job is unique, they should all follow the same basic process: assess, plan, prepare, execute. We could spend a whole day just covering the elements involved in determining the causes of deterioration and selecting repair methods (Assess and Plan). We’re going to very briefly touch on these steps. We’ll focus more of our time on the second half of the repair process, which is preparing the surface and executing the repair.

## Slide 5: Assessing the Condition
Cause | Effect | Size/depth | Location/accessibility
Notes: Step 1: Assessing the Condition
Large spalled area underside of a deck (left)
Spall on grade on a deck ramp (right)
Obviously we can’t perform field tests from a picture, but what can you visually assess here about the cause, effect, size, depth, location and accessibility?
Thinking ahead to the Planning step - Consider the cause, type, size/depth, location/accessibility, temperature/climate, urgency, structural needs, and aesthetics to begin developing a repair strategy. (Make some assumptions for these example since we do not have all of the information necessary to plan a repair.)
Let’s take a closer look at what goes into planning a repair, aka engineering the appropriate solution.

## Slide 6: Planning the Repair
Assessment
User Needs
Repair Analysis
Useful life
Urgency
Cost
User technical performance requirements
Aesthetics
Cause
&
Scope
Effect
&
Scope
Structural needs
Effect of repair on structure
Constructability
Environment
Safety
Repair Strategy
Source: Emmons, P. H. (1993). Concrete repair and maintenance illustrated. Kingston, MA: R.S. Means Company
Placement method
Material
Structural support design
IT’S COMPLICATED
Notes: Step 2: Planning the Repair
A lot goes into designing the proper repair. A comprehensive evaluation must be conducted including both the cause and effect of the deterioration. The results of the evaluation, together with the users needs and requirements, form the necessary external information to begin the design process. The final design presents a solution based on considerations of durability, constructability and compatibility with the existing structure.
Again, we could spend a whole day on this step alone – but we’re not!

## Slide 7: Surface Preparation
Determine layout and sawcut perimeter
Remove concrete
Clean reinforcing steel and remaining concrete
Protect reinforcing steel
Notes: Step 3: Preparing the Surface
(The first part of surface prep I’m assuming Bosch is covering in some depth, and we can jump into priming the reinforcing steel after the concrete is removed and surface is cleaned. If not, un-hide the following three slides)
Note – steps to Undercut reinforcing steel and Repair reinforcing steel would be added if needed before protecting reinforcing steel.

## Slide 8: Determine Layout
Mark perimeter of repair area minimizing corners
Delaminated, Cracked Areas
Incorrect Layout
Recommended Layout
Notes: Mark the perimeter of the repair area. Preferable layout will result in simple geometric shapes with few reentrant corners. The illustration of an incorrect layout shows areas where cracks can develop.

## Slide 9: Concrete Removal
Sawcut the perimeter, remove loose or delaminated concrete
Notes: Sawcut the perimeter of the repair. To avoid damaging reinforcement, the sawcut should not be deeper than the cover over the reinforcement. If the delamination is caused by corrosion, but the area of corroded reinforcing isn’t apparent, use chipping hammers to expose the reinforcement until areas of uncorroded bars are found. Then sawcut an area that encompasses the boundaries of corrosion that have been established.
Remove delaminated concrete, undercut reinforcing steel, remove additional concrete as required to provide minimum required thickness of repair material.
Perform initial concrete removal with either 15-lb or 30-lb jackhammers. Jackhammers larger than 30 lb may cause damage to reinforcement, reinforcement bond to surrounding concrete, and remaining concrete. Use 15-lb jackhammers for final removal and detailing around the reinforcing steel.
There are many options for doing surface preparation depending on the extent that deteriorated concrete needs to be removed. Sometimes it requires full depth replacement.
If exposed bars are corroded, concrete surrounding the bar should be fully removed to expose the corroded bar, regardless of how much of the bar is corroded. Removals around the bar should allow the hand to pass under the bar. Clearance around the bar should be approximately 3/4 in. Undercutting will provide clearance for under bar cleaning and full bar circumference bonding to surrounding concrete, and will secure the repair structurally.
If corroded bars are found and the bars have loss of cross section, a structural engineer should be consulted.

## Slide 10: Clean Steel & Concrete
Clean exposed concrete and reinforcing bars
Notes: Final cleaning of the exposed reinforcement and concrete is required. Use of high-pressure water or abrasive blasting is required to remove loose and bond-inhibiting materials. Surface must be sound, clean, free of bond-inhibiting materials, with aggregate bonded to cement matrix
An open pore structure is a critical bonding mechanism. Make sure pores are not clogged with dust, debris, or water. Methods to open pores:
  Hydroblasting
  Shotblasting
  Abrasive blasting
  Vacuum

## Slide 11: Protect Reinforcing Steel
In repair situations where additional corrosion protection is needed
  Promote adhesion, dry rapidly, and can be shop or field applied
    FX-406 Zinc-Rich Primer
      Single-component
      Provides sacrificial protection
    FX-408 Zinc-Rich Epoxy Primer
      Two-component
      Provides both barrier and sacrificial protection
Metal Primers
Notes: In repair situations where additional reinforcement protection is needed.

## Slide 12: Protect Reinforcing Steel

## Slide 13: Bond to Existing Concrete
Increase adhesion of repair material to existing substrate
Existing
Bonding Agent
New
Bonding Agents
    FX-Bondcrete Latex Bonding Agent and Admixture
    FX-752 Epoxy Bonding Agent
    FX-792LPL Long Pot Life Epoxy Bonding Agent
Notes: Step 4: Executing the Repair
Our bonding agents are designed to improve the bond between freshly placed repair mortars or concrete mixes and existing concrete. The appropriate bonding agent is chosen based application requirements.
    FX-Bondcrete Latex Bonding Agent
      Single-component latex bonding agent. It also improves the bond of thin-set patching, masonry mortars and stucco mixes as an integral admixture.
    FX-752 Epoxy Bonding Agent
      100% solids, two-component, moisture-tolerant epoxy system
    FX-792LPL Long Pot Life Epoxy Bonding Agent
      Two-component, 100% solids, moisture-tolerant epoxy resin

## Slide 14: Bond to Existing Concrete

## Slide 15: Place Repair Material
Placement method depends on the situation (dry packing, form and pour, overlays...)
Steps typically include mixing, placing, finishing, and curing
Repair Mortars & Repair Epoxies
    FX-263 Rapid-Hardening Vertical/Overhead Repair Mortar
    FX-928 Fast-Setting Concrete Mix
    FX-763 Low-Modulus Trowel-Grade Epoxy
Notes: The placement method is usually determined in the repair strategy. Make sure to consider questions: Will the necessary equipment be accessible? Are there experienced contractors available? Placement method may need to be adjusted based on these and other factors.
In general, the placement steps typically include mixing, placing, finishing, and curing.
Here are just three examples of products:
    FX-263 Rapid -Hardening Vertical/Overhead Repair Mortar
      Cementitious, single-component, fiber-reinforced, polymer-modified, silica fume-enhanced, structural repair mortar with integral corrosion inhibitor
    FX-928 Fast-Setting Concrete Mix
      Single-component, rapid-hardening concrete mix with integral corrosion inhibitor designed for horizontal and formed vertical repairs where a quick turnaround with minimal downtime is required
    FX-763 Low-Modulus Trowel-Grade Epoxy
    Two-component, 100% solids, moisture-tolerant, non-sag epoxy designed for vertical, horizontal, and overhead applications and uses

## Slide 16: Place Repair Material

## Slide 17: Basic Repair Process
Condition Assessment
Removal & Surface Preparation
Repair Analysis, Strategy & Design
Repair Execution
ASSESS
PLAN
PREPARE
EXECUTE
1
2
3
4
Notes: We covered this process very quickly, but remember that an effective repair MUST address the root cause of the original problem. Bosch has tools for concrete removal and proper surface preparation. Simpson offers metal primers, bonding agents, and repair materials to complete the repair.

## Slide 18: Repair, Protection and Strengthening Systems for Concrete and Masonry
Project Types:
Repair and Protection
Bonding Agents, Coatings, Cementitous, Epoxy, Polymer, Polyurethane, FX-70®
Strengthening
FRP, FRCM
Pile repair
Bridges
Infrastructure
Water and Wastewater
Notes: Here’s a high-level overview of what our Repair, Protection and Strengthening Systems (RPS) line looks like and what type of project types to look for. Our business is broadening.
As part of general concrete repair, we talked about metal primers, bonding agents, and repair mortars (patch and spall repair). We also offer crack injection materials, grouts, joint sealants, coatings and membranes.
(Have participants refer to their RPS product guides.) Let’s take a look at the Product Guide.

## Slide 19: Product Guide
  Grouped by application type
  General Concrete Repair
  Performance Coatings
  Crack Repair
  Joint Sealing
  Grouting
  Underwater Repair Materials
  Rail Products
  Specialty Products
  Tools and Accessories
Notes: The RPS Product Guide is organized by application type. So all of the products needed for certain applications can be found in one area.
General Concrete Repair should look familiar because that’s what we just covered. You’ll also see
  Performance Coatings
  Crack Repair
  Joint Sealing
  Grouting
  Underwater Repair Materials
  Rail Products
  Specialty Products
  Tools and Accessories

## Slide 20: Product Guide
Navigation – pg. 5
Numerical index by formulation
Product Group sections
Notes: Turn to page five to see that you can look for product guide information by using the index if you already know the product formulation (ex: FX-501), or you can find products by looking at type of application (i.e. Performance Coatings).

## Slide 21: Product Guide – Page Layout
Product sub-type
Product model # & title
Product description
Application information
Product features
Packaging information
Notes: (Bullets and callouts appear with each click)
Page Walk-through – Let’s take a look at what you should know about each page

## Slide 22: More Information
Product Guide
Online resources
  Technical Data Sheets
  Jobsite Assessment Tools
  Safety Data Sheets
Call an SST Rep
Repair, Protect, and Strengthen
Simpson Strong-Tie has become a trusted manufacturer of chemical, mechanical, direct-fastening, and carbide drill bits and accessories since entering the market in 1994. Now in our 20th year, we continue to expand to provide the most comprehensive product offering to serve infrastructure, commercial, industrial and residential construction markets. These innovative products are the result of more than 40 years of laboratory development, field study and contractor input and have passed the rigorous performance and quality assurance testing you have come to expect from Simpson Strong-Tie. We will continue to expand upon this line of repair, protection and strengthening products and provide our customers with industry leading jobsite, technical and customer support.
Notes: We didn’t have a lot of time to go in-depth, but use the Product Guide to learn more about the many RPS solutions offered. You can also go to strongtie.com for tech data sheets, jobsite assessment tools, safety data sheets, and product information. Finally, talk to your SST technical sales rep to have your questions answered.

## Slide 23
Questions?
Notes: Are there any questions?